## Slide 1: Present status and future prospects of the application of liquid metals for plasma-facing components in magnetic fusion devices
TOFE-2014
Nov. 9-14th
Anaheim, USA
Yoshi Hirooka（NIFS), G. Mazzitelli (ENEA), S. Mirnov (TRINITY),
M. Ono (PPPL), M. Shimada (JAEA), F. L. Tabares (CIEMAT)

## Slide 2: Table of contents
Background
  Plasma-wall boundary control effects
  Technical issues with solid metal PFCs (for ITER and beyond)
  Potential issues with liquid metal PFCs
Liquid metal PFCs in fusion device and lab. experiments
  Confinement experiments with liquid metal PFCs
  Laboratory experiments with liquid metal samples
Innovative liquid metal PFC concepts
  TEMHD-concept driven by JxB
  ACLMD-concept driven by JxB
  Conclusion

## Slide 3: “Chicken-Egg” Boundary control effect ① Reduced edge density => improved core confinement
After J.D.Strachan, Nucl. Fusion 39(1999)1093.
Supershots in TFTR
Super dense core in LHD
After N. Ohyabu et al., PRL97(2006)055002.

## Slide 4: “Chicken-Egg” Boundary control effect ② Improved core confinement => reduced edge density
Edge transport barrier
NBI-heating start
Density increase
Edge density
decrease
Temperature
increase
ETB
After F. Wagner et al. PRL 49(1982)1408
After F. Wagner et al. PRL 53(1984)1408
L-to-H mode transition with ETB in ASDEX

## Slide 5: Technical issues with present-day PFCs
W-armor + Cu alloy heat sink
  Divertor heat flux：10~20MW/m2
Plasma current~15MA
Heating power～100MW
  PFC power width: λq= ~ 5㎜
DEMO-divertor
W-armor + F82H heat sink
  Max. heat flux：～8MW/m2
  Plasma current~20-30MA
  Heating power~500MW
  PFC power width: λq= ~ 1㎜
Need for an innovative PFC ! !
Possible metals and/or alloys:
Ga（Tm=29.8℃, Z=31）
Li(Tm=186℃, Z=3）
Sn（Tm=231℃, Z=50）
Li17Pb83（Tm=235℃, Z=69*）
ITER-divertor
After Loarte presented at 2014 PSI-conf.

## Slide 6: DBTT(~400ｄ℃) cracking on tungsten-PFC
Thermal cycle cracking
15MW/m2
50MW/m2
Low H retention =>high recycling
Hydrogen-implantation cracking

## Slide 7: Potential issues on liquid metal PFC concepts
After A. Ying (UCLA)
B
v
MHD drag
After M. Ono (PPPL NSTX-U)
Valves
Impurities
EM Pumps
Liquid Lithium Divertor Tray (LLDT)
200°C – 450°C
Divertor Heat and Particle Flux
Lithium Radiative Mantle
B
?

## Slide 8: CPS-limiter(s) in T11, FTU, TJ-II, etc.
Langmuir probes
Thermocouples
Heater electrical cables
Spray vaporized lithium over a large area of the first wall for gettering (reduced recycling)
Capillary effect to pump liquid lithium from the reservoir behind the mesh
Li-coatings have induced H-mode in TJ-II
After Sanchez et al. Nucl. Fusion4(2009)104018.
ETB(?)

## Slide 9: Lithium emission-collection “loop” in T11 After Mirnov, paper presented at the IAEA-FEC 2014

## Slide 10: Active radiative liquid lithium divertor After Ono et al. FED(2014)in press.
Radiative Liquid Lithium Divertor
“RLLD” implemented in a reactor

## Slide 11: POP on particle control by Li-gettered MS-PFC (Presented at ANS-TOFE, 2002)

## Slide 12: Power/particle handling issues with the Liquid Lithium Divertor
Li + O2 ⇒ LiO2
H2+ 1/2O2 ⇒ H2O
Li + H2O ⇒ Li(OH) + 1/2H2
LLD in NSTX
Buoying impurities: LiO2, LiOH
Surface heating->Natural convection
Natural
convection
Forced
convection
=> High recycling
Kugel et al. Fusion Eng. Des. 87(2012)1724
LLD

## Slide 13: Steady state plasma device at NIFS: VEHICLE-1
Plasma parameters:
ne: ~1010 cm-3
Te: 3~4 eV
Ion flux : ~1 x1016 cm-2s-1
Species mix modelling

## Slide 14: Liquid metal stirring experimental setup

## Slide 15: Hydrogen and helium solubility in lithium
Hydrogen solubility in lithium
Helium solubility in lithium

## Slide 16: Liquid stirring effects on hydrogen recycling
Hirooka et al. Fusion Eng. Des. (2014) in press

## Slide 17: Liquid stirring effects on helium recycling
Hirooka et al. Fusion Eng. Des. (2014) in press

## Slide 18: TE-MHD: JxB force-driven liquid metal PFC
After Jaworski (PPPL)
PoP experiments in HT-7(@AS-IPP)
JxB force
Zuo et al. Fusion Eng. Des. (2014) in press

## Slide 19: ACLMD: JxB forced convection liquid metal PFC
After Shimada and Hirooka
PoP experiment at NIFS
Nucl. Fusion 54 (2014) 122002
Current externally controllable!!
Convection externally controllable!!
Liquid temp. externally controllable!!
Liquid metal: Ga67 In20.5 Sn12.5

## Slide 20: Potential issues with ACLMD
Electro-chemistry effects
Standard electrode potential*: Eo
Li Eo=-3.045V
Al Eo=-1.67V
Cr Eo=-0.74V
Fe Eo=-0.44V
Ni Eo=-0.24V
W Eo=-0.58V
Sn Eo=-0.14V
H Eo=0.0V
Ag Eo= +0.79eV
Au Eo= +1.52eV
* ΔGo =-zFEo ( z: # of electrons
F: Faraday’s const.)
Joule heating effects
JxB force heating power: J・V
In the case of our PoP exps. on ACLMD:
  J~20[A]
  V~2.9[V] when rotation starts at 6 rpm
  P~60[W]
The temperature of Ga67 In20.5 Sn12.5 alloy (320cc) was felt about 50oC. After a while, however, the rotation stops, which indicates a temperature effect on electrochemical properties of (liquid) metals.

## Slide 21: Summary and technical implications
Present status of liquid metals and/or their vapor/deposits to be used as PFCs has been reviewed with the emphasis on power and particle handling requirements.
Implications are: liquid metals needs to be flowing with forced convection for better temperature control and hydrogen absorptivity.
Several Innovative concepts to overcome the MHD drag have been proposed, showing successful PoP. However, there is a long way to go to reach the same level of technical maturity as the present-day divertor concept. We must count on the next generation scientists!