## Slide 1: An investigation of low recycling, low collisionality and high performance with lithium conditioning in LTX-β
Dec – 9, 2021
Anurag Maan
Dennis Boyle
Dick Majeski
George Wilkie
Manaure Francisquez
Elizabeth Perez
Robert Kaita
Santanu Banerjee
William Capecchi
Ron Bell
NSTX-U / Magnetic Fusion Science Meeting
Vlad Soukhanovskii
Chris Hansen
Laura Zhang
Evan Ostrowski
Bruce Koel
Drew Elliott
Shigeyuki Kubota
David Donovan
Ted Biewer
Filippo Scotti

## Slide 2: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 3: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 4: LTX and LTX-beta overview
Parameters |  | LTX | LTX-β | Planned
Major Radius | R0 | 34 – 40 cm |  | 
Minor Radius | a | 20 – 26 cm |  | 
Vacuum Pumping |  | 6,000 L/s | 12,000 L/s | 13,000 L/s + Ti
Li Heat/Evap/Cool time |  | 200/10/100 mins | 10/10/10 mins | 5/5/5 mins
Toroidal Field | BT | 0.17 – 0.2 T | 0.3 T | 0.34 T
Plasma Current | Ip | < 85 kA | 140 kA | 150 kA
Plasma Duration | tshot | < 50 ms | < 50 ms | 100 ms
Beam Power | PNBI | 0 | 300 - 700 kW | 300 - 700 kW
Beam Duration | tNBI | 0 | 5-6 ms | 10-30 ms
1.4 m

## Slide 5: LTX – Key experimental result – Hot edge, collisionless SOL, improved confinement
Notable SOL features (D. Majeski, PoP, 2017)
Low collisionallity (banana regime) – neo-classical effects cannot be ignored in the SOL
Edge density reduces after lithium application and edge temperatures increase
Large connection length (5-10 m)
Pitch angle scattering times >> SOL transit times -> SOL particles are likely mirror confined
Need kinetic modelling of the SOL – but sheath limited models for ‘back of the envelope’ estimates
D. Boyle et. al., Phys Rev Letters, 2017
Also recently reproduced by SPECTOR General Fusion

## Slide 6: Improved performance in the presence of oxidized lithium
Improved performance in the presence of oxidized lithium puzzling.
Previous hypothesis Li + H => LiH
Key results
    Flat temperature profiles
    Oxidized lithium
M. Lucia, PhD Thesis, 2015
R. Kaita et. al., Fusion Engr. and Des., 2017
Li2O, LiOH

## Slide 7: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 8: X-Ray photoelectron elemental and chemical composition
Elemental composition
  Photoionization cross-sections
Chemical composition
  Binding energies
XPS broad energy range scan for Lithium on LTX-β
8
XPS Narrow Energy range O(1s) scan of a Lithium Sample
O(1s)

## Slide 9: LTX XPS data did not have high enough resolution to ID compounds
Elemental and Chemical composition
  Photoionization cross-sections
  Binding energies
No chemical composition information available.
Conclusions based solely on elemental abundances
NEED HIGH RESOLUTION!!

## Slide 10: Sample Exposure Probe – Enable high resolution XPS measurements
A Maan, et. al., Review of Scientific Instruments 91, 026104 (2020)

## Slide 11: Lithium and plasma exposure

## Slide 12: Lithium and plasma exposure

## Slide 13: Transfer and Scan

## Slide 14: Transfer and scan
14

## Slide 15: Transfer and scan
15
MAPP - LTX
PHI + SEP – LTX-β

## Slide 16: Lithium PFC Evolution for LTX-β
A. Maan et al., IEEE Transactions on Plasma Science, vol. 48, no. 6, pp. 1463-1467.

## Slide 17: Lithium PFC Evolution and Chemical Species Identification

## Slide 18: Lithium PFC Evolution and Chemical Species Identification

## Slide 19: Lithium PFC Evolution and Chemical Species Identification
  Surface rich in chemical species
  Best case scenario
  Primary surface constituent Li2O
  LiOH grows after Li2O
  First in-vacuo observation of lithium compound evolution in a tokamak

## Slide 20: Lithium PFC Evolution and Chemical Species Identification
  Surface rich in chemical species
  Best case scenario for current experiments
  Primary surface constituent Li2O
  LiOH grows after Li2O
  First in-vacuo observation of lithium compound evolution in a tokamak

## Slide 21: Lithium PFC Evolution and Chemical Species Identification
  Surface rich in chemical species
  Best case scenario for current experiments
  Primary surface constituent Li2O
  LiOH grows after Li2O
  First in-vacuo observation of lithium compound evolution in a tokamak

## Slide 22: Lithium PFC Evolution and Chemical Species Identification
  Surface rich in chemical species
  Best case scenario for current experiments
  Primary surface constituent Li2O
  LiOH grows after Li2O
  First in-vacuo observation of lithium compound evolution in a tokamak

## Slide 23: How does surface oxidation affect plasma performance?
LTX-beta old lithium coating passivated with Argon backfill+vent
Baked to 200 C, wait to cool down and make plasma
Deposit lithium
Wait for long time scales ~ 1 week
Make plasma
Compare

## Slide 24: Plasma performance improves
Current and duration improve
Oxygen line emission goes down
Lithium line emission increases
Probe density decreases and temperature increases after gas puff

## Slide 25: Plasma performance improves
Current and duration improve
Oxygen line emission goes down
Lithium line emission increases
Probe density decreases and temperature increases after gas puff

## Slide 26: Direct measure of changes in surface and co-relation with plasma performance
First Direct in vacuum characterization of lithium compounds on a tokamak PFC
Lithium Oxide seems to improve performance by reducing oxygen impurity content as opposed to LiOH.
A Maan et al 2021 Plasma Phys. Control. Fusion 63 025007

## Slide 27: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 28: Low field side Single Langmuir Probes
NEW Single tipped, swept with 1kHz triangular wave – 200 V peak to peak
Mounted off-midplane to avoid run-away electrons during low density phases
1.91mm[0.075 in]
Tungsten probe tip (1 mm)
Boron Nitride insulator
TZM Sheath
Steel mounting piece
MACOR Insulator

## Slide 29: Poloidal Lyman-Alpha array
Light reflection from metal PFCs complicate recycling measurement
20 Element AXUV photodiode array to measure Lyman-Alpha emission
Crucial for recycling measurement
Low reflection from Li and Li compounds at 121.6 nm

## Slide 30: Supersonic Gas Injector - Design
Proximity of supersonic gas injector (SGI) valve to nozzle eliminates edge cooling from residual gas in line for conventional gas puffer
High levels of conventional gas puffing is incompatible with a hot – low recycling edge
Improvements include a double walled heatshield and a vortex tube for hot shells operation
Mounted vertically through a shell penetration closer to the high field side
SGI Nozzle
Final bellows mounted assembly
SGI Nozzle
Heat shield
PV-10 housing
Cooling channel
T/C
Gas inlet
Trigger
SGI location

## Slide 31: Lithium Evaporators for LTX-beta – Mark-I
  Few minutes per evaporation
  1-1.5 Hr between evaporation and run
  Point source approximation predicts most of the PFC covered

## Slide 32: Lithium Evaporators for LTX-beta – Mark-II
  New lithium evaporators.
  Few minutes per evaporation
  1-1.5 Hr between evaporation and run
  Point source approximation predicts most of the PFC covered

## Slide 33: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 34: Plasma performance improves with thicker lithium coatings
Old Li*
322 mg Li
863 mg Li
Core density and temperatures at peak density t=468 msec
Old Li*
322 mg Li
863 mg Li
  Plasma current increases
  Peak density reduces
  Density decay time reduces
  Shots last longer
  Temperature profiles relax and become more flat
  Edge densities drop

## Slide 35: Effective particle confinement time reduces with increased lithiumization
  Efficient edge fueling with a supersonic gas injector enables an effective particle confinement to be estimated.
  where,
Old Li
322 mg Li
863 mg Li

## Slide 36: Effective particle confinement time reduces with increased lithiumization
  Efficient edge fueling with a supersonic gas injector enables an effective particle confinement to be estimated.
  where,
Old Li*
322 mg Li
863 mg Li

## Slide 37: Lyman Alpha array intensity progressively reduces with more lithium
  Lyman-alpha array signal shows progressive reduction with increasing lithiumization for the same fueling sequence
  The decay rate of signal intensity after a puff is also seen to reduce with more lithium
  Comparing Lyman alpha signal intensities across different timepoints at similar line averaged density also shows a similar reduction, indicating a trend independent of density.
Most Li
Least Li

## Slide 38: Lyman Alpha array intensity progressively reduces with more lithium
  Lyman-alpha array signal shows progressive reduction with increasing lithiumization for the same fueling sequence
  The decay rate of signal intensity after a puff is also seen to reduce with more lithium
  Comparing Lyman alpha signal intensities across different timepoints at similar line averaged density also shows a similar reduction, indicating a trend independent of density.

## Slide 39: SOL profile measured using Thomson scattering and Langmuir probe data
  SOL density and temperature is approximated using an exponential decay fit using data from the main TVTS system and the low field side Langmuir probe.
  Extrapolation of density decay from fit to TVTS data agrees well with the probe data
  Probe temperature measurement likely specious for hot edge, new low field side TS optics should solve this!
Old Li
322 mg Li
863 mg Li

## Slide 40: DEGAS2 analysis yields low recycling
  Ignoring ion trapped fractions yields really low recycling coefficients
  Overall trend of reduced recycling with increased lithiumization persists
  The trend agrees with other observations that indicate reduced recycling.
    Reduced Lyman alpha emission reduction
    Quicker density decay
    Flat temperature profiles

## Slide 41: Overview
Lithium Tokamak eXperiment (LTX) - Context
Surface analysis for Lithium Tokamak eXperiment-β
  Sample Exposure Probe
  Lithium Plasma Facing Component (PFC) Evolution
  Plasma Performance and correlation with PFC evolution
Recent diagnostic and operational upgrades to LTX-beta
  Langmuir probe
  Lyman-alpha array
  Supersonic Gas injector
  Newer lithium evaporators
Performance improvement with increased lithiumization
  Flat temperatures
  Effective particle confinement time
  Reduced Lyman-alpha emission
  DEGAS2 analysis
New Gkeyll simulations inform on the impact of collisionality with increased lithiumization

## Slide 42: Gkeyll used for gyrokinetic simulations of open field lines in the SOL
Full simulation domain
Simulation domain collapsed on a poloidal cross-section
Gkeyll evolves the long-wavelength gyrokinetic equation.
Solved in 1D along the field line coupled with a field equation for potential.
Necessary due to long collisional mean-free paths in the SOL relative to the connection length
Free parameter and convergence scans completed, able to match experimental data at midplane

## Slide 43: Collisionality scans show reduced particle and heat flux with as collisionality is reduced
Numerically swept collision frequency
Midplane density increases with reduction in collisionality but edge density reduces
Temperature rises with reduction in collisionality
Particle and heat flux go down
Old Li*

## Slide 44: Collisionality scans show reduced particle and heat flux as collisionality is reduced
Numerically swept collision frequency
Midplane density increases with reduction in collisionality but edge density reduces, likely indicates trapping
Temperature rises with reduction in collisionality
Particle and heat flux go down
Introduction of lithium reduces collision frequency, note, the magnitudes on y axis are different
Old Li*
863 mg

## Slide 45: Summary
First direct in vacuum identification of Lithium compounds on a fusion reactor first wall
Li in tokamak Plasma Facing Components (PFCs) oxidizes to Li2O, which maintains favorable performance (like Li) by reducing impurities and recycling
Multiple diagnostic and operational upgrades to LTX-beta enable recycling analysis and SOL characterization
Recycling analysis with DEGAS2 and other indicators show reduced recycling coefficients as more lithium is evaporatively deposited on LTX PFC
New Gkeyll analysis shows favorable reduction in particle and heat flux to the walls with more lithiumization

## Slide 46: Thank you

## Slide 47: Backup

## Slide 48: DEGAS2 analysis yields low recycling
  TRANSP indicated energy confinement time is within an error bar of the effective particle confinement time for lowest recycling case.
  Comparison of energy confinement time at peak density shows reduced energy confinement, likely due to much lower density for the low recycling case (almost half)
  Comparison of energy confinement time at constant density shows improved energy confinement with reduced recycling.
Peak density
Constant density

## Slide 49: Low field side Single Langmuir Probes
Last low field side probe blew up! – Spewed Aluminum everywhere

## Slide 50: TRANSP shows low collisionality core plasma
Old Li*
322 mg Li
863 mg Li