## Slide 1: Stuck in the Rough: How Aging Reactor Walls May Exhibit Lower Erosion [DOE Highlight]
Shota Abe1,2, C.H. Skinner1, A. Liu3,1, J. Garcia4,1, Z. Lin2, S. Bringuier5, T. Abrams5, and B.E. Koel1
1 Princeton Plasma Physics Laboratory, USA
2 Department of Chemical and Biological Engineering, Princeton University, USA
3 Department of Nuclear, Plasma, and Radiological Engineering, University of Illinois at Urbana-Champaign, USA
4 Department of Mechanical Engineering, San Diego State University, USA
5 General Atomics, San Diego, USA
NSTX-U / Magnetic Fusion Science Meeting, PPPL, NJ, USA, March 6, 2023
This work is from: “Computational investigation of ion incident angles and material erosion of micro-rough graphite and silicon carbide divertor surfaces” S. Abe et al., Phys. Plasmas 29, 102503 (2022), APS Invited
sabe@pppl.gov

## Slide 3: Surface structure is a key parameter of fusion divertor PMI
Strong dependency on incident angle
Polar Angle (θ)
Sputtering Yield [atoms/ion]
Behrisch, Eckstein, “Sputtering by Particle Bombardment“ (2007)
Rough surfaces of PFC
Abrams et al., NF 2021
θ
Ion
SiC
Graphite
Impurity & T trapping
Erosion
Shadowing
Effects of rough surfaces on erosion and ion-shadowing are investigated
→
→

## Slide 4: Key parameter: Surface Inclination Angle Distribution (SIAD)
Surface Inclination Angle δ
Key parameter
Local incident ion angle
Cupak 2021 Appl. Surf. Sci.
θ
Ion

## Slide 5: Workflow using two models
Lasa and Coburn
github.com/ORNL-Fusion/
LMPS
Incident ion angle distribution (IAD)
Input surface data
Skinner
NME 2019
NSTX-U graphite
(confocal microscopy)
Input
Input
Output
Erosion
Ion shadowed area
Micro-Patterning and Roughness (MPR)
Input
(1)
(2)
Difference from previous works
(1) Calculated IADs using verified sheath length
(2) Real (measured) surface data

## Slide 6: 4 divertor surfaces were scanned for computational study
DIII-D DiMES
Graphite
130x130 μm,
(i) 40x25 μm
RRMS = 1.9 μm,
(i) 0.1 μm
NSTX-U
Graphite
85x65 μm,
(ii) 16x16 μm
RRMS = 1.3 μm,
(ii) 0.3 μm
DIII-D tile
SiC
1250x950 μm
RRMS = 6.6 μm
Before exposures
DIII-D tile
SiC
1200x1200 μm
RRMS = 8.0 μm
After exposures
Measured by
confocal microscopy
subarea
subarea

## Slide 7: IAD calculation inputs and assumptions
Potential profile
LMPS = 3×ρi (ρi: Ion gyro radius)
(-3 < < -2.4)
Borodkina CPP 2016
Stangeby 2000 IOP Publishing
Incident ion angle distribution (IAD) calc.
This factor ”3” was determined in Abe et al., Nucl. Fusion 62, 066001 (2022)
Equation-of-motion (EOM)
F = e(E + v×B)
Initial velocity distribution
, : Maxwell-Boltzmann ()
Collisionless: LMPS (~mm) << λMFP (~cm)
λChargeExchange ~ 0.1 mm when ne = nn = 1021 m-3 (ITER)
Hence, we examined ne = 1019-1020 m-3
v0

## Slide 8: Takeaway1: General IADs at divertor surface were also found
Incident ion angle distribution (IAD) calculation
Polar IADs are sensitive to B-field incident angle α
α = 88.5° case was verified by micro-trench experiment
Incident ion: D+
Te = 10-30 eV
ne = 1019-1020 m-3
B = 1-5 T
Plasma parameters
Abe 2021 NME
Those IADs are global for any divertor plasmas having plasma parameters shown on the left
Result
Result

## Slide 9: DiMES graphite surface was experimentally benchmarked
Exp.
Skinner
NME 2019

## Slide 10: Erosion and ion shadowed area were quantified
Large shadowed area in micro-valley
Redeposition << Erosion
Species redeposited at neighboring area
~5%

## Slide 11: Erosion and ion shadowed area were quantified
Erosion
Ion Shadowed Area
Large shadowed area in micro-valley
Redeposition << Erosion
Species redeposited at neighboring area
~5%

## Slide 12: Erosion and ion shadowed area were quantified

## Slide 13: Erosion and ion shadowed area were quantified
Erosion
Ion Shadowed Area

## Slide 14: Rrms is NOT good parameter to explain PMI! SIAD is!!
Erosion
Ion Shadowed Area
More roughness ≠ more shadow
Go to next slide: SIAD (Surface Inclination Angle Distribution) is the best parameter
More roughness ≠ less erosion
Local incident ion angle (LIIA) predicts the erosion (75% of smooth surface sputtering yield)
SIAD can be used to determine LIIA
Database sputtering yield
Behrisch, Eckstein, “Sputtering by Particle Bombardment“ (2007)
Bringuir NME (2019)

## Slide 15: Takeaway2: General results were found for erosion and redeposition predictions on any divertor surfaces
Incident ion: D+
Te = 10-30 eV
ne = 1019-1020 m-3
B = 1-5 T
Erosion
Ion Shadowed Area
Local Incident Ion Angle
Impurity Redeposition
Tritium Trapping
To predict
To predict
Surface Inclination Angle δ
Key parameter
Local incident ion angle
Cupak 2021 Appl. Surf. Sci.

## Slide 16: Summary
Acknowledgements: Ane Lasa, Jonathan Coburn, Christopher P. Chrobak, Jerome Guterl, Igor Bykov, Eduardo Marin, Arturo Domingues, DeeDee Ortiz, Koel (PU) group
This work is supported by U.S. DOE under DE-AC02-09CH11466, DE-FC02–04ER54698, DE-AC02-09CH11466, and Princeton’s High Meadows Environmental Institute
The Surface Inclination Angle Distribution (SIAD) is the key parameter to predict the Local Incident Ion Angle (LIIA) and ion shadowed area on rough surfaces.
Using LIIA and sputtering yield data of a flat surface, we can predict the erosion of rough surfaces.
Global IADs were calculated as a function of B-field incident angle.
Thank you!

## Slide 17: IAD becomes broader due to surface structure
Flat surface

## Slide 18: Calculation of local incident ion angle