## Slide 1: Summary and updates of the micro-trench method for impurity deposition and incident ion angle measurements
Shota Abe
Staff Research Physicist, Princeton Plasma Physics Laboratory, USA
NSTX-U / Magnetic Fusion Science Meeting
PPPL, NJ, USA, March 6, 2023

## Slide 2: Keyword: Shadowing
Shadowing is useful
Sundial has measured
time & season since 1500 BC
Wikipedia

## Slide 3: Keyword: Shadowing
Shadowing is useful
Sundial has measured
time & season since 1500 BC
Sun location
Wikipedia

## Slide 4: Keyword: Shadowing
Incident
photon
direction
Shadowing is useful
Sundial has measured
time & season since 1500 BC
Sun location
Incident photon angles
Azimuth ϕ
Polar (Altitude) θ
Time
Time & season
Wikipedia

## Slide 5: Shadowing affects erosion (melting) patterns on the surface
reddit.com, @u/banana-nou
reddit.com
reddit.com, @u/DankPastaMaster

## Slide 6: Incident ion angle measurement

## Slide 7: Micro-trench technique uses ion shadowing effect to reveal D ion incident direction
Micro trenches fabricated by focused ion (Ga) beam (FIB)
S1
Micro-
trenches
30x30x4 µm deep
Si sample disc
45º
view
SEM before exposure
Top
view

## Slide 8: Micro-trench technique uses ion shadowing effect to reveal D ion incident direction
Micro trenches fabricated by focused ion (Ga) beam (FIB)
S1
Micro-
trenches
30x30x4 µm deep
Si sample disc
45º
view
Reported
SEM before exposure
Top
view
ϕ
θ
amazon.com
C.H. Skinner

## Slide 9: Micro-trench technique uses ion shadowing effect to reveal D ion incident direction
Micro trenches fabricated by focused ion (Ga) beam (FIB)
S1
Micro-
trenches
Shadowed
Sputtered
30x30x4 µm deep
Si sample disc
D Ions
Al C
Micro-trench
45º
view
Reported
SEM before exposure
from graphite walls
C ions
D Ions
1-3% of ion flux
Top
view
S. Abe 2021 NME 27 100965

## Slide 10: Micro-trench technique uses ion shadowing effect to reveal D ion incident direction
Micro trenches fabricated by focused ion (Ga) beam (FIB)
S1
Micro-
trenches
Shadowed
Sputtered
Si sample disc
D Ions
Al C
Micro-trench
from graphite walls
C ions
D Ions
1-3% of ion flux
reddit.com, @u/DankPastaMaster
S. Abe 2021 NME 27 100965

## Slide 11: Engineered samples exposed on DiMES
DiMES
LP
DiMES head location
OSP
S1
Micro-
trenches
Si sample disc
DIII-D attached deuterium L-mode plasma
Te ~ 30 eV, ne ~ 1019 m-3, I┴ ~ 1022 cm-2s-1,
texp = 10 s , Tsurf < 250 ºC
Plasma parameters
IB
C - Graphite
DiMES head
DIII-D

## Slide 12: Impurities are redeposited and trapped in the D ion shadowed area
R
BT
Dark area = impurity deposition
Before exposure
x
y
BT
Tilted view
µm
x
y
After exposure
SEM images

## Slide 13: Impurities are redeposited and trapped in the D ion shadowed area
R
BT
Dark area = impurity deposition
Before exposure
x
y
BT
Tilted view
µm
x
y
After exposure
SEM images
Erosion
Deposition

## Slide 14: Polar and azimuthal ion incident angles measured by analyzing the impurity deposition pattern
µm
R
BT
C ~ 30 at. %
SEM image after exposure
C EDS intensity (deposition)
µm
Max
Int.
[a.u.]
Energy dispersive X-ray spectroscopy
C concentration in shadowed area > 10x
Gross deposition rate ~ 10 nm/s
Abe 2021 PS

## Slide 15: Polar and azimuthal ion incident angles measured by analyzing the impurity deposition pattern
µm
R
BT
C ~ 30 at. %
SEM image after exposure
C EDS intensity (deposition)
µm
Max
Int.
[a.u.]
= -40º
80º
First detailed experimental measurement
What is the important physics behind this observation?
Energy dispersive X-ray spectroscopy
Abe 2021 NME
Abe 2022 Nucl. Fusion

## Slide 16: Sheath length determination

## Slide 17
’Reverse engineering’ of sheath potential (length) from the measured ion incident angle
α
B
Sheath potential (E-field) affects the ion trajectory
Plasma parameters
Ion velocity
Measured
Incident
ion angle
Measured
When α < 5º, wide electric sheath, magnetic pre-sheath (MPS) or Chodura sheath : LMPS ~ k×ρi
LMPS is an input parameter of PMI codes: ERO etc

## Slide 18
’Reverse engineering’ of sheath potential (length) from the measured ion incident angle
α
B
Sheath potential (E-field) affects the ion trajectory
Plasma parameters
Ion velocity
Measured
Incident
ion angle
Measured
k: Free parameter
When α < 5º, wide electric sheath, magnetic pre-sheath (MPS) or Chodura sheath : LMPS ~ k×ρi
LMPS is an input parameter of PMI codes: ERO etc

## Slide 19
’Reverse engineering’ of sheath potential (length) from the measured ion incident angle
α
B
When α < 5º, wide electric sheath, magnetic pre-sheath (MPS) or Chodura sheath : LMPS ~ k×ρi
LMPS is an input parameter of PMI codes: ERO etc
Sheath potential profile by kinetic simulation
MPS (No DS)
DS boundary
Coulette PPCF 2016
α = 2º
10º
90º
k = 3
Borodkina CPP 2016
k: Free parameter
Sheath potential (E-field) affects the ion trajectory

## Slide 20: Ion trajectories calculated for various sheath lengths
DIII-D attached deuterium L-mode plasma
Te ~ 30 eV, ne ~ 1019 m-3, α = 1.5º
E
Free parameter
k×ρi

## Slide 21: Ion trajectories calculated for various sheath lengths
IADs by Equation-of-Motion
First experimental determination of the tokamak sheath length
agreed with k ~ 3 of kinetic model prediction
Polar
Azim.
k = 0.5
Coulette PPCF 2016
1
1
0.5
2
4
k = 3
Exp.
Exp.
E
k = 3
Abe. 2022 Nucl. Fusion
k×ρi
DIII-D attached deuterium L-mode plasma
Te ~ 30 eV, ne ~ 1019 m-3, α = 1.5º

## Slide 22: Deposition and erosion measurements

## Slide 23: Micro-trench also measured Si erosion and C deposition rates
Si surface
Ga layer
C deposition
D+
Original trench surface
~30 nm (TRIM)
Cx+
Ga
C
BT

## Slide 24: Micro-trench also measured Si erosion and C deposition rates
Ga
C
BT
Si surface
Ga layer
C deposition
Erosion
Rate
by AFM
Reference
Original trench surface
~30 nm (TRIM)
Gross C deposition rate (without D sputtering) by AFM
3.5 nm/s
Si erosion rate
C deposition rate
11 nm/s
Result of L-mode discharges

## Slide 25: Ongoing/upcoming works

## Slide 26: Gross deposition measurement of IPD coatings in DIII-D
USN
LSN
A. Bortolon et al 2019 Nucl. Mater. and Energy 19 384-389
R. Lunsford et al 2019 Nucl. Fusion 59 126034
F. Effenberg et al 2022 Nucl. Fusion 62 106015
IPD
IPD
IPD
Effective (net) B:C film growth rate ~1-2 nm/s (0.1 nm per mg of B) was found in DIII-D
Gross deposition rate? MT can answer
We will apply the micro-trench method for boron and lithium IPD this year in DIII-D
along with composition analysis of the deposited layers
RTWC with boron powder

## Slide 27: Applications for different plasma parameters
We did the model validation with D plasmas
How about other ion species?
H and He plasma measurements as a collaboration with LHD, NIFS (Prof. Masuzaki) in 2024
LHD has FIB for micro-trench fablication, EDS for composition analysis
Answers C gross deposition
Deep trench gives C incident angle
Adjustable angle of the LHD probe head lets us investigate different B field incident angle (DIII-D we tried only α=88°)
DIII-D plans H plasma discharge in June 2023
H-mode exposure as collaboration with Sandia (Dr. Coburn) in April 2023
Tokitani 2011

## Slide 28: Investigations on Incident Ion Angle, Sheath and Roughness Effects for better PMI understanding
Equation-of-motion
MPR
Monte-Carlo
Jhovanna Garcia, Euichan Jung, Anurag Maan (PPPL)
Ion Angle Probe (IAP)
Confocal Microscopy
on SS LTX Wall
MPR Calculation
Microtrench
Sample
Langmuir
Prove
Heater
IAP
30 μm
Expected Deposition Pattern
Incident Ion
Angle
Microtrench Method
Incident Ion Angle
Li deposition Rate
Net Li Sputtering Rate
S. Abe, PoP,NF,NME,PS 2021-2022
MPR Calculation
Sputtering Yield on Rough-surface
Shadowed Area

## Slide 29: sabe@pppl.gov
Acknowledgements: Bruce E. Koel (PU) group, C.H. Skinner, I. Bykov, Y.W. Yeh, A. Lasa, J. Coburn, D.L. Rudakov, C.J. Lasnier, H.Q. Wang, A.G. McLean, T. Abrams, C. Chrobak, R. Akhmechet, Z. Lewicka, D. Barth, J. Schreiber, G. Cheng, D. Buchenauer, J. Whaley, R. Kolasinski, F. Zhao, B. Harrop, D. Coulette, G. Manfredi
Micro-trench technique for:
Incident ion angle measurement
Impurity deposition (gross) rate measurement
Erosion rate measurement
References:
DIII-D DiMES micro-trench
S. Abe et al. 2022 Nucl. Fusion 62 066001
2021 Phys. Scr. 96 124039
2021 Nucl. Mater. Energy 27 100965
Thank you!