## Slide 1: Recent progress on investigations into plasma-lithium surface interactions in LTX-β (ISLA-7 Encore)
Shota Abe1,2, Anurag Maan1, Evan T. Ostrowski2, Promise O. Adebayo-Ige3, Kaifu Gan3, Euichan Jung1,
Jhovanna Garcia1,4, Brady Moore1,5, Sophie M. Redd1,6, Zihan Lin2, Dennis P. Boyle1, Predrag Krstic7,
Rajesh Maingi1, Brian Wirth3, Bruce E. Koel2, and Dick Majeski1
1Princeton Plasma Physics Laboratory, USA 2Department of Chemical and Biological Engineering, Princeton University, USA
3University of Tennessee, Knoxville, USA 4San Diego State University, USA 5University of Illinois, Urbana-Champaign, USA
6University of Colorado Boulder, USA 7TheoretiK, USA
NSTX-U / Magnetic Fusion Science Meeting (B318 / Zoom)
PPPL, NJ, USA, June 26, 2023

## Slide 3: Lithium as plasma-facing material (PFM)
High H retention ~0.4-0.8
Low recycling
Light mass (Li = 7 amu)
Liquid state (> 455 K) = No cracks
Low energy loss
Fewer instabilities
1.6 m
LTX-β
PPPL
Benefits of Lithium walls
Low H recycling enables
Flat
Te
Experiment
Boyle, PRL 2017
NSTX-U
PPPL
Properties of Li as PFC needs to be studied
Flat temperature profile
Jaworski, Nucl. Fusion 2013

## Slide 4: Lithium as plasma-facing material (PFM)
1.6 m
LTX-β
PPPL
Boyle, PRL 2017
Maximum Parameters |  | LTX | LTX-β
Major Radius | R | 40 cm | 
Minor Radiues | a | 26 cm | 
Toroidal Field | BT | 0.18 T | 0.3 T
Ohmic Flux Swing | ΔΦ | 75 mV∙s | 120 mV∙s
Plasma Current | Ip | 85 kA | 135 kA
Flattop Duration | tflat | ~15 ms | ~35 ms
Electron Temperature | T | ~250 eV | ~400 eV
Ion Temperature | Ti | ~100 eV | ~200 eV
Plasma Pressure | p | ~0.5 Pa | ~1.5 kPa
Energy Confinement | τE | ~2 ms | ~5 ms
Neutral Beam Current | Inbi | - | ~35 A
Neutral Beam Energy | Enbi | - | 13-20 keV
Neutral Beam Duration | tnbi | - | 5-10 ms
Wall Temperature | Twall | Up to 500 K (liquid) | 
100% Li coated plasma-facing surface
Li Evaporator in LTX-β
Fresh vs. Old Li
Investigating plasmas for
Liquid vs. Solid Li
Anurag Maan, Dennis P. Boyle, Dick Majeski (PPPL)

## Slide 5: Hot shell operation in 2023
Anurag Maan, Dennis P. Boyle, Dick Majeski (PPPL)
Maan, IEEE 2020
Solid
2023
Liquid

## Slide 6
Li target
Sample Exposure Probe (SEP)
Vacuum suitcase for sample transfer
LTX-β
Surface Science and Technology Laboratory
Bruce E. Koel lab
IAC&PRISM
Plasma performance affected by wall conditions
Li evaporation
H retention using TPD
XPS analysis
SIMS analysis
Sputtering
Retention
Emissivity
Li deposition
Impurity
SAM imaging
HR-XPS analysis for detailed chemical state
Controlled experiment under ultra-high vacuum (10-10 Torr)
Li target
Post-mortem surface analysis
Sample preparations
Predrag Krstic
(TheoretiK)
Molecular-Dynamics calculations
Sputtering and Retention

## Slide 7
★
★
★
★
★
★
★
IAC&PRISM

## Slide 8
Li target
Sample Exposure Probe (SEP)
Vacuum suitcase for sample transfer
LTX-β
Surface Science and Technology Laboratory
Bruce E. Koel lab
IAC&PRISM
Plasma performance affected by wall conditions
Li evaporation
H retention using TPD
XPS analysis
SIMS analysis
Sputtering
Retention
Emissivity
Li deposition
Impurity
SAM imaging
HR-XPS analysis for detailed chemical state
Controlled experiment under ultra-high vacuum (10-10 Torr)
Li target
Post-mortem surface analysis
Sample preparations
Predrag Krstic
(TheoretiK)
Molecular-Dynamics calculations
Sputtering and Retention

## Slide 9: Sample Exposure Probe (SEP) enables in-vacuo sample transfer
Maan, PhD thesis 2019
Sample Exposure Probe (SEP)
Maan RSI 2020
Transfers sample at P0 ~ 10-9 Torr
Heating capability up to 900 K
[New!] Temperature Programmed Desorption (TPD) for surface composition and H retention analysis
1” Diameter
Sample Head
Turbo Pump
Gate Valve
SS Sample Head
LTX-β
Evan T. Ostrowski (Princeton U.) and Anurag Maan (PPPL)
[Ongoing]
Sara Sawford (SULI 2023)
Powder sample manipulator

## Slide 10: Sample Exposure Probe facilities to investigate experimental Li studies
Maan, PhD thesis 2019
Sample Exposure Probe (SEP)
SEP
XPS analysis chamber
[New!] Sample Exposure Station
w/ electron cyclotron resonance (ECR) plasma source
SEP
Li target
SEP
Maan RSI 2020
LTX-β
Surface Science and Technology Laboratory
Surface Science and Technology Laboratory

## Slide 11: X-ray Photon Spectroscopy (XPS) revealed surface composition of the LTX-β Li surface
SEP
XPS analysis chamber
Kolasinski “Surface Science” 2012
Measured
Known
Determined
Surface Science and Technology Laboratory
Evan T. Ostrowski (Princeton U.)
LiOH
Li2O
Temperature changes surface composition
! Old data !

## Slide 12: Temperature Programmed Desorption (TPD) for H retention analysis
QMS
SEP
Heated
Li target
Desorbed H2
LTX-β
H plasma
Measured retained H by heating up Li sample after exposures
Surface temperature during exposure affects H retention behavior
Evan T. Ostrowski (Princeton U.)
458 K
300 K
! Old data !

## Slide 13: Investigations on Incident Ion Angle, Sheath and Roughness Effects for better PMI understanding
Equation-of-motion
MPR
Monte-Carlo
Jhovanna Garcia and Euichan Jung (PPPL)
Ion Angle Probe (IAP)
Confocal Microscopy
on SS LTX Wall
MPR Calculation
Microtrench
Sample
Langmuir
Prove
Heater
IAP
30 μm
Expected Deposition Pattern
Incident Ion
Angle
Microtrench Method
Incident Ion Angle
Li deposition Rate
Net Li Sputtering Rate
S. Abe, PoP,NF,NME,PS 2021-2022
MPR Calculation
Sputtering Yield on Rough-surface
Shadowed Area

## Slide 14
Li target
Sample Exposure Probe (SEP)
Vacuum suitcase for sample transfer
LTX-β
Surface Science and Technology Laboratory
Bruce E. Koel lab
IAC&PRISM
Plasma performance affected by wall conditions
Li evaporation
H retention using TPD
XPS analysis
SIMS analysis
Sputtering
Retention
Emissivity
Li deposition
Impurity
SAM imaging
HR-XPS analysis for detailed chemical state
Controlled experiment under ultra-high vacuum (10-10 Torr)
Li target
Post-mortem surface analysis
Sample preparations
Predrag Krstic
(TheoretiK)
Molecular-Dynamics calculations
Sputtering and Retention

## Slide 15: Sample exposure probe facilities to boost the speed of experimental Li studies
Maan, PhD thesis 2019
Sample Exposure Probe (SEP)
SEP
XPS analysis chamber
SEP
Li target
SEP
Maan RSI 2020
Surface Science and Technology Laboratory
[New!] Sample Exposure Station
w/ electron cyclotron resonance (ECR) plasma source

## Slide 16: New chamber for plasma exposures, surface analysis, and Li target preparation
Sample Exposure Station (SES)
± Ions
Energy
analyzer
ECR
Plasma
Hiden
IDP
SEP
D2, H2, He, Ar, Ne
20-2000 eV
Ion exposures
SEP compatibility to introduce LTX-β sample
In-vacuo Li deposition (100 nm/min)
Sputtering yield measurements
Secondary ion mass spectrometry (SIMS)
Thermal programmed desorption (TPD)
IR window for emissivity measurements
Shota Abe and Euichan Jung (PPPL)
Base pressure: 10-9 Torr
[Ongoing]
Amanda Roman (SULI 2023)

## Slide 17: In-vacuo thick Li film deposition for plasma exposure studies
Sample Exposure Station (SES)
± Ions
Energy
analyzer
ECR
Plasma
Hiden
IDP
D2, H2, He, Ar, Ne
20-2000 eV
Euichan Jung, Amanda Roman, Brady Moore (PPPL)
Base pressure: 10-9 Torr
SEP
Thermocouple
Heating Coil
Before
After
Only 5 min duration between
deposition and experiment
Experiments on pure liquid Li
Li deposition at 2.5” distance

## Slide 18: Experimental Measurement of Li+ Sputtering Yields
* QMS intensity normalized by the ion current at the target (measured/calibrated by Faraday cup)
* D3+ and H3+ are dominant species
(ED = ED2+/3, ID = ID2+×3)
7Li+
D bombardment ejects more (~2x) Li+ than H
Hot surface (460 K) changes Li+ ejection behavior
H and D will sputter Li+ even for E < 100 eV
He can cause large sputtering even for E < 100 eV
For E > 200 eV, yields for Ar / Ne ion bombardment are 10x higher than H and D ion bombardments
Ionic state of sputtered Li is ~60%
Allain, NF 2002
Li(60%)-C(2%)-O(38%)-H on SS
At.% measured by XPS
Target (300 or 460 K)
Maan, IEEE 2020
, which will be back to the surface by sheath.
Shota Abe (PPPL)

## Slide 19: O ions ejected as negative ions
OH- ejection due to sputtering
O ejection with attached D (OD-)
No OH- nor OD- ejections observed
Water ion OHD- ejection
Shota Abe (PPPL)
Drawn to the plasma by sheath

## Slide 20: H- ion ejection was observed
> 0.1 [H-/H] at low incident energy
Shota Abe (PPPL)
Drawn to the plasma by sheath
[Ongoing]
Andrea Hernandez (SULI 2023)
Secondary ion emission from
Li, B, W, C etc.

## Slide 21: Retarding Field Energy Analysis of Ejected Ions
Sputtered Li+ ions: 1-20 eV
Incident ion species
7Li+
Reflected ion E << Sputtered ion E
40%
<E>
Sputtered positive Li ions will be trapped in the sheath (~100 eV)
<E>
Shota Abe (PPPL)
MD
unpublished

## Slide 22: Retarding Field Energy Analysis of Ejected Ions
Sputtered Li+ ions: 1-20 eV
Incident ion species
7Li+
Sputtered positive Li ions will be trapped in the sheath (~100 eV)
<E>
Shota Abe (PPPL)
MD
unpublished
Ion bombardments work for surface cleaning
Abe et al., Journal of Fusion Engineering, ISLA-7 special issue (2023), Under review

## Slide 23: Emissivity determination for accurate wall temperature measurements
Ideal black body
Measured
Emissivity
Emissivity can be different for different materials and chemical states
IR temperature measurement relies on the emissivity value
Emissivity for Li2O was determined
Pure Li including liquid state and different compositions (C/N/D) are being investigated
Promise O. Adebayo-Ige, Kaifu Gan, Brian Wirth (University of Tennessee, Knoxville)
Oxidized Li

## Slide 24
Li target
Sample Exposure Probe (SEP)
Vacuum suitcase for sample transfer
LTX-β
Surface Science and Technology Laboratory
Bruce E. Koel lab
IAC&PRISM
Plasma performance affected by wall conditions
Li evaporation
H retention using TPD
XPS analysis
SIMS analysis
Sputtering
Retention
Emissivity
Li deposition
Impurity
SAM imaging
HR-XPS analysis for detailed chemical state
Controlled experiment under ultra-high vacuum (10-10 Torr)
Li target
Post-mortem surface analysis
Sample preparations
Predrag Krstic
(TheoretiK)
Molecular-Dynamics calculations
Sputtering and Retention

## Slide 25: Detailed understanding of chemical states and evolutions of lithium surface
e-
e-
Absorbed XY Molecule
ΔE = Ei - Es
Ei
Es
X
Y
Li
Li
Li2O suggested
No O2
Artificially oxidized Li target on graphite
Wulfsberg 2016
O 1s
3 nm Li
H2+ ion exposure 1015 H/cm2
44-hr resting in vacuum
LiOH
Li2O
Li/Ni(111)
Dosed @ 300 K
LEED @ 300 K
E = 63 eV
LEED
HR-XPS
Maan 2020
Low-res
HR Electron Energy Loss Spectroscopy (HREELS)
Evan T. Ostrowski and Zihan Lin (Princeton U.)

## Slide 26: Molecular-Dynamics Calculation Revealed Several PMI parameters
Predrag Krstic (TheoretiK)
Sputtering and Reflection (= 1 - Retention) Yields
Ion energy: 0.03-100 eV
Projectile species: H, D, and T
Target: Li, LiH, Li2O, and LiOH
Target Temperature: 300 – 600 K
Liquid (Amorphous)
Previous exp.
MD Results
Sputtering Yield
Sputtering Yield
Crystal
Lab. experiments are on going to catch up the speed of calculations
Krstic, JNM 2022
Krstic, JNM 2022

## Slide 27
Acknowledgements: Koel (PU) group, LTX-β (PPPL) group, and SULI program (PPPL)
This work is supported by U.S. DOE under DE-SC0019308, DE-AC02-09CH11466, DE-AC52-07NA27344, and DE-SC0008309
LTX-β
Dr. Anurag Maan, Dr. Dennis P. Boyle, Dr. Dick Majeski (PPPL)
Sample exposure probe (SEP)
Evan T. Ostrowski, Prof. Bruce E. Koel (Princeton U.)
Dr. Shota Abe, Dr. Anurag Maan (PPPL)
Micro-trench ion incident angle measurement
  Jhovanna Garcia, Euichan Jung, Dr. Shota Abe (PPPL)
  Prof. Bruce E. Koel (Princeton U.)
Thank you!
Ion sputtering Experiment
Dr. Shota Abe (PPPL), Prof. Bruce E. Koel (Princeton U.)
HR-XPS
Evan T. Ostrowski, Zihan Lin, Prof. Bruce E. Koel (PU)
Emissivity measurement
Promise O. Adebayo-Ige, Kaifu Gan, Brian Wirth (UTK)
Rajesh Maingi (PPPL)
Molecular-dynamics calculations
  Dr. Predrag Krstic (TheoretiK)
sabe@pppl.gov