## Slide 1: Characterization of boronized graphite in NSTX-U and its effect on plasma performance
F. Bedoya, J.P. Allain, R. Kaita and C.H. Skinner
59th Annual APS DPP Meeting
Milwaukee, WI
Oct 23rd – Oct 27th 2017

## Slide 2: Motivation – Oxygen retention
Oxygen concentration reduction in PFCs with boronization improves performance.
Low oxygen concentration following boronization
Improved plasma performance on similar scenarios
MAPP XPS data obtained at NSTX-U
Further studies in the laboratory (post-mortem and control) to test this hypothesis
IP (kA)
NBI (MW)

## Slide 3: Samples made from NSTX-U tiles (post-mortem)
Tiles location
A18, Center Stack (CS) Shoulder
B17, Inner Lower Divertor (ILD)
C18, Outer Lower Divertor (OLD)
Core samples
CS -Shoulder
Inner LD
Outer LD

## Slide 4: Experimental methods
Analysis
Chamber
MAPP Facility
Materials analysis in NSTX-U
Post-mortem and Controlled experiments at University of Illinois
IGNIS Facility
Ar+,D+

## Slide 5: Ion-Gas-Neutral Interactions with Surfaces (IGNIS) Facility
True in-situ, in-operando analysis of surfaces.
Chemistry analysis (HR-XPS, HR-ISS) at NAP (UHV to 1 mTorr OP).
Wide experimental parameters space:
  Temperature LN to 1000 oC.
  Plasma irradiations; noble and reactive gas (250 eV – 2 keV)

## Slide 6: Chemical identification of components via XPS
Emission of photoelectrons under incident soft X-ray beam
Probe top 1 – 10 nm of sample
Elemental identification in survey scans
Region scans allow quantitative analysis (at.%)
Oxygen
Carbon
Survey scan
Region scans
h
e-

## Slide 7: XPS OLD sample – Highest oxygen and boron concentration at OSP region
High presence of oxides throughout the whole experiment
Highest boron concentration of all cores (~20%) in analyzed depth (~100 nm)
Also highest oxygen concentration in depth ( as much as 40%)
Core C18 – OLD sample
As is
1x1015 Ar+/cm2
3.5x1017 Ar+/cm2

## Slide 8: XPS ILD sample – Evidence of presence of impurities on surfaces in PFR region
High presence of oxides throughout the whole experiment
Presence of a new XPS peak, attributed to Cl, possible NSTX-U impurity
B-B and B-C (non-oxidized) states observable following Ar+ irradiation
Core B17 – ILD sample
As is
1x1015 Ar+/cm2
3.5x1017 Ar+/cm2

## Slide 9: XPS CS sample – Different chemistry in CS and LD
Initial high presence of oxides (lower concentration than other cores)
B-B and B-C states visible after Ar+
Post-cleaning state has the closest resemblance to post-boronized state from MAPP
Core A18 – CS Sample
As is
1x1015 Ar+/cm2
3.5x1017 Ar+/cm2

## Slide 10: XPS CS sample - D+ Irradiation drives oxidation
Deuterium irradiation drives oxidation of the B coatings, the oxides can be easily removed with additional irradiation.
Similar to what we observed in NSTX-U with MAPP !!
Core A18 – D+ Irradiation
6x1016 D+/cm2
3.5x1017 Ar+/cm2
2.0x1017 Ar+/cm2

## Slide 11: Conclusions
Samples manufactured from tiles extracted from NSTX-U were characterized post-mortem using XPS and ion beam etching
The boron concentrations on the three samples were different, implying possible non-uniform deposition during boronization.
D+ irradiation of clean post-mortem sample showed similar behavior to that observed in MAPP:
  Deuterium ions driven oxidation
  Plasma (Ar+) induced sputtering and oxides removal