## Slide 1: Active conditioning of ASDEX-Upgrade tungsten PFCs through boron particulate injection (FIP/2-3)
R. Lunsford1 , V. Rohde2, A. Bortolon1, A. Drenik2, R. Dux2, A. Herrmann2,
A. Kallenbach2, R. M. McDermott2, R. Maingi1, D.K. Mansfield1, A. Nagy1,
R. Neu2, E. Wolfrum2 and the ASDEX-Upgrade team
27th IAEA Fusion Energy Conference, 22-27 October 2018, Gandhinagar, India
1Princeton Plasma Physics Laboratory, Princeton, NJ, USA
2Max Planck Institute for Plasma Physics, Garching, Germany

## Slide 2: “Real-Time” boronization through powder injection
Plasma assisted wall conditioning uses solid B compounds instead of toxic and explosive B2D6 gas
Deposition of B powders extends the effective lifetime of boronization coatings
  Allows density-controlled, high-purity plasmas with reduced wall fueling and mitigated High-Z impurity sources
  Maintains controlled wall conditions over a run campaign
  Could be used to provide active boronization for future long pulse discharges

## Slide 3: Outline
Experimental Apparatus
Boron Injection Experiments
  Boron Nitride Injection Series
  Boron Injection Series
Conditioning Effects

## Slide 4: Impurity powder dropper (IPD)
Multi-impurity injection system based on linear piezoelectric powder feeder
4 feeders with separate reservoirs (30 ml) around central drop tube
Tested with multiple materials
  B, BN, Li, Si, SiC, Sn…
  particle size 5-100 μm
  calibrated rates 2-200 mg/s
Injection calibrated with accelerometer, optical flow-meter confirms mass injection rate
Boron Nitride BN
A. Nagy et al., Rev. Sci. Instr. at press 2018

## Slide 5: IPD installed atop AUG during Fall 2017
2.5 m drop tube connects IPD with crown of AUG discharge
Chamber 1 loaded with 5 mm BN powder
Chamber 2 loaded with 70 mm B powder
BN
B

## Slide 6: Outline
Experimental Apparatus
Boron Injection Experiments
  Boron Nitride Injection Series
  Boron Injection Series
Conditioning Effects

## Slide 7: B/BN injected into conformal discharges to enhance coating
Wall-conditioning discharge with conformal shape
  SOL surfaces parallel to antenna limiter
ELM-y H-mode discharges with IP = 0.8 MA, BT = 2.5 T, PNBI = 10 MW, PEC = 0.8 MW, ne = 6.5x1019 m-3
Conditioning effects inferred from visible spectroscopy
  Line emission from BII, OII, WI assumed representative of wall source
  Views for divertor (DVL) and limiter (LVL)
W impurity influx from ICRH antenna limiter inhibits low-collisionality operation
  D2 puff required to maintain robust ELM frequency
DVL
ICRH antenna
limiter
IPD
LVL

## Slide 8: Wall conditioning by B powder injection
Experiment scheduled to provide maximum chance to observe changing wall conditions (directly before standard D2B6 boronization)
9 conditioning discharges with BN or B
  Constant injection rate for 1-3 s @ 2-75 mg/s
6 test discharges w/o IPD
  Interleaved to assess changing wall conditions
3 attempts at ELM-suppression with RMP after completing conditioning discharge sequence
  scenario tests access to low collisionality
Total ~330 mg of B introduced in AUG
ASDEX-U Shot Number
34790
34800
34810
34820
34830

## Slide 9: Outline
Experimental Apparatus
Boron Injection Experiments
  Boron Nitride Injection Series
  Boron Injection Series
Conditioning Effects

## Slide 10: Boron nitride injection series
BN input from 3.8-4.9 s
N radiation dominates, No N latency
B radiation at limiter and divertor
ASDEX Discharge | Injection Species | Quantity of boron injected (atoms) | Cumulative boron injection
34796 | BN | 1.7x1019 | 1.7x1019
34798 | BN | 1.7x1020 | 1.9x1020
34799 | BN | 3.5x1020 | 5.4x1020
34801 | BN | 1.6x1021 | 2.2x1021
34803 | BN | 1.4x1021 | 3.6x1021
Intensity (a.u.)
Nitrogen Intensity

## Slide 11: BN increases confinement similar to N2
34801
34802
34799
BN, 52 mg/s
BN, 9 mg/s
#34802 : Control Discharge
#34799 : 9 mg/s
  5% increase of ne and Prad
  Stored energy WMHD unchanged
#34801 : 52 mg/s
  ne +25% and Prad +80%
  WMHD increases until core mode destabilized (N~2.7)
  Confinement improvement associated with pedestal recovery
  Greater coupling to discharge than seen with N2 gas puff
A. Bortolon et al., Submitted J. Nucl. Mater. Energy 2018

## Slide 12: Outline
Experimental Apparatus
Boron Injection Experiments
  Boron Nitride Injection Series
  Boron Injection Series
Conditioning Effects

## Slide 13: Metallic Boron Injection Series
Pure B input from 3.8-7.9 s
Less additional radiation, stable discharge
CEX shows B fully penetrates discharge
ASDEX Discharge | Injection Species | Quantity of boron injected (atoms) | Cumulative boron injection
34808 | B | 9.6x1020 | 4.5x1021
34809 | B | 3.6x1021 | 8.1x1021
34825 | B | 1.0x1022 | 1.9x1022
B5+ concentration

## Slide 14: Metallic Boron Injection Series
ASDEX Discharge | Injection Species | Quantity of boron injected (atoms) | Cumulative boron injection
34808 | B | 9.6x1020 | 4.5x1021
34809 | B | 3.6x1021 | 8.1x1021
34825 | B | 1.0x1022 | 1.9x1022

## Slide 15: Boron injection well tolerated by plasma
ELMy H-modes, fELM~70-100 Hz
  10 MW NBI, 1.2 MW ECRH
  D2 fueling throughout
#34825 : B injection, 75 mg/s
  Modest ~5% increase of ne
  Oscillations due to fluctuations in drop rate (B clumping)
Prad increase by 20%
No effect on stored energy WMHD
34802
34825
B 75 mg/s
A. Bortolon et al., Submitted J. Nucl. Mater. Energy 2018

## Slide 16: Outline
Experimental Apparatus
Boron Injection Experiments
  Boron Nitride Injection Series
  Boron Injection Series
Conditioning Effects

## Slide 17: Low-density test shot shows slight improvement
Due to wall conditions test discharge scenario is unstable w/o gas puff
  Core MHD
  Prad runs away
  Radiative collapses → disruption
After BN/B injection MHD persists
  Prad run away is avoided
  Plasma sustained to completion
34810
34797
34800
A. Bortolon et al., Submitted J. Nucl. Mater. Energy 2018
#34797 : ~3.7 x 1018 B atoms injected
#34800 : ~1.3 x 1020 B atoms injected
#34810 : ~5.8 x 1021 B atoms injected

## Slide 18: Wall condition observables improve during test-shot series
Impurity source estimated from time-average of line emission
  BII, OII and WI
B from limiter increases → B coating
O from limiter decrease → O gettering
W source decreases for >100 mg B
Similar trends observed in divertor
A. Bortolon et al., Submitted J. Nucl. Mater. Energy 2018

## Slide 19: Boron injection assists successful RMP ELM suppression
Total boron injected : 330 mg
#34826 : Attempted ELM-suppression
D2 puff stopped at t=2.25s
n = 2 RMP from 2.5 – 7 s
Full-shot ELM suppression achieved
  Sufficient ne pump-out maintained
  3 consecutive discharges
Slow increase in Prad and W radiation
  Impurity sources recovering on discharge time-scales
Need to confirm B injection is responsible
IP(MA)
PAUX(a.u.)
Da(a.u.)
H98
ne( x1019 m-3)
PRAD(a.u.)
WMHD(MJ)
Magnetic Perturbations
ELMs suppressed
#34827 & #34829
suppressed also
34826

## Slide 20: Summary
Boron Nitride:
  Observed increased B & N flux from limiters & divertor
  Prad increased by > 100% at highest rates
  At high injection rates, confinement and stored energy increased by 20-30%, as observed with N2 puffing
  Crashed at bN > 2.7
Elemental Boron
  Observed increased B flux from limiters & divertor
  Prad increased by 50% at highest rate
  Discharge stable, B injection limit not reached
BN and B powder both successfully injected into auxiliary heated AUG plasmas

## Slide 21: Conclusions and Outlook
Initial AUG experiments suggest that boron powder injection can be used to augment borization coating during tokamak operation
  Successful modification of edge impurity levels
  Successful access to low density for RMP ELM suppression
  Upcoming experiments planned to corroborate results and optimize technique
Particulate wall conditioning could aid steady-state operation where initial coatings will erode rapidly
IPD has been/is being installed on other devices
  DIII-D results to be presented at APS 2018
  Successful horizontal B4C injection into W7-X
  Experiments on EAST, KSTAR to address applicability to long pulse operation

## Slide 22
Thank you!
IPD

## Slide 23
Supplemetal Information

## Slide 24: Performance enhancement observed with BN similar to N2 gas puff Greater coupling to discharge with smaller Nitrogen quantity Reduction in Ammonia quantity Suggestive of NH3 mitigation possibilities for JET & ITER to prevent tritium sequestration Full behavior not well understood, further study required
Inner Divertor – Partial Pressure of Residual Gasses
10-10
10-8
10-6
10-4
Partial Pressure [a.u.]
10-10
10-8
10-6
10-4
Partial Pressure [a.u.]
Nitrogen
Ammonia
# 34267, Gaseous N2
# 34800, No BN
# 34803, BN
# 34809, B
RGA Comparison of BN injection and N2 gas puff
0
5
10
15
20
Time(s)
25
0
5
10
15
20
Time(s)
25