## Slide 1: The IFMIF Target Facility Engineering Design and the Validation of Key Issues within the IFMIF/EVEDA Project
F. Groeschel
On behalf of the IFMIF-EVEDA Project Team
2nd International Symposium on Lithium Applications
Princeton, 27-29 April 2011

## Slide 2: Outline of talk
Scope of IFMIF and of the IFMIF/EVEDA Project
IFMIF Loop Concept and ELiTe Loop for off-beam tests
Li Target Assemblies and validation of free surface flow
Li purification system and its validation
Li safety issues for IFMIF and ELiTe
Summary and conclusions

## Slide 3: IFMIF “Artist View” (CDR, 2003)
Ion Source
RF Quadrupole
Post Irradiation Experiment Facilities
High Energy Beam transport
Li Target
Li Loop
Test Modules inside Test Cells
Drift Tube Linac
0 20 40 m

## Slide 4: Principle of IFMIF
L
M
H
Accelerator (125 mA x 2)
Test Cell
Beam shape:
200 x 50 mm2
High (>20 dpa/y, 0.5 L)
Medium (>1 dpa/y, 6 L)
Low (<1 dpa/y, > 8 L)
100 keV
HEBT
Source
140 mA D+
LEBT
RFQ
MEBT
RF Power System
Half Wave Resonator Superconducting Linac
Lithium Target
25±1 mm thick, 15 m/s
Chart: Neutron Energy (MeV)
Typical reactions
  7Li(d,2n)7Be
  6Li(d,n)7Be
  6Li(n,T)4He
5 MeV
9 14.5 26 40 MeV

## Slide 5: Objectives of the IFMIF/EVEDA Project
Produce a detailed, complete and fully integrated engineering design of the International Fusion Materials Irradiation Facility and all data necessary for future decisions on the construction, operation, exploitation and decommissioning of IFMIF
Validate continuous and stable operation of each IFMIF subsystem by designing, manufacturing and testing scalable models to ensure engineering feasibility
Article 1 of Annex 1 of BA Agreement, February 2007

## Slide 6: Engineering Validation & Engineering Design Activities
Lithium Test Loop (scale 1/3)
Validation goals
Stable free surface Li flow in the target assembly
Achievement of low impurity levels of oxygen, nitrogen, hydrogen (< 10 wppm)
IFMIF/EVEDA Accelerator Building
Rokkasho
Oarai

## Slide 7: IFMIF Li loop baseline concept (2003)
Quench Tank
Deuteron Beams
EM Pump
HX(Li / Organic Oil)
Dump Tank
HX(Organic Oil / Water)
Li flow
Cold Trap
T Hot Trap
Loop properties | 
Li inventory | 4.5 to
Li flow rate | 130 l/s
Piping | 8/10“
Operating temperature | 250-350C
Heat to be removed | 10 MW
Secondary cooling | oil
Tertiary cooling | water

## Slide 8: ELiTe loop layout
Li inventory | 2.5 to
Li flow rate | 50 l/s
Piping | 6/8“
Design pressure | 7.5 bar(g)
Design temperature | 400C
Operating temperature | 250-350C
Heat to be removed | 150 kW
Design acceleration | 0.36g h/0.24g v
Structural material | AISI 304
Scaling in flow rate 1:2.6
NPSH requires similar height as IFMIF
Air cooler, no secondary loops
Bypass branch for target assembly to facilitate start of flow through target assembly
Purification system integrated in main structure
Purification branch with small EMP (10 l/s)

## Slide 9: Target assembly concepts
The target assembly conditions and shapes the flow to form a 260 mm wide, 25 mm thick Li jet flowing in an concavely shaped open channel
Three concepts have been developed in the past
TA with integrated backwall (tested in ELS, ISTC)
Lipseal welded and clamped backplate concept
Bayonet backplate concept
Two concepts are realized and tested in the ELiTe loop
Integrated backwall TA made of stainless steel
Bayonet backplate concept made of F82H/Eurofer
Li jet width | 100 mm
Li jet height | 25±1 mm
Flow channel curvature | 250 mm  7 m
Flow veolcity | 10-20 m/s
Nozzle | Shima two stage
Nozzle reduction ratio | 10:2.5.:1
Nozzle and channel roughness | < 3 mm
Vacuum pressure | 10-4 to 10-3 Pa
Argon pressure | < 0.1 Mpa(a)

## Slide 10
Stereo-Scopic Imaging System
HSV
Electro-contact probe
Li free surface flow validation
How to assure stable Li free surface flow in the beam footprint; i.e. thickness variation < ±1 mm
How to manage Li evaporation from the free surface
Li deposition sampler
Quartz microbalance
Diagnostics developed by Osaka University and qualified in Osaka loop
CFD modeling by several institutes

## Slide 11: Lithium Purification in IFMIF and Validation
Lithium has to be purified
  To maintain the liquid metal properties (viscosity, avoid plugging)
  To mitigate corrosion/erosion. Nitrogen enhances corrosion in stainless steels by forming a soluble CrLiN-compound
  To reduce the radioactive inventory and the limit the radiation field around the loop. Production of 3H is about 7.5 g/fpy and of 7Be is about 1.5 g/fpy in IFMIF. Corrosion products from the target assembly and others passing through the target assembly are activated
Purification system
  Cold trap operating below the loop temperature
  Nitrogen hot trap operating at 580-600C
  Hydrogen isotopes trap operating at 280-300C
  On-line composition monitors (hydrogen, resistivity, plugging meter)
  Li samplers for off-line analysis
Target impurity level design values
  10 wppm for H, N and corrosion products
  1 wppm for 3H
11

## Slide 12: IFMIF cold trap and ELiTe validation
Cold trap design is based on Na experience
Main source term is
  Initial oxidized steel surface (1 g/m2)
  Recontamination of surfaces during maintenance
Intermittent operation could be envisable
Trapping of Be during beam operation is not very effective due to low temperature gradient to main loop
12
ELiTe
Li in (210 C)
Li out (190 C)
Air out (55 C)
Air in (30 C)
Li drain
IFMIF
Properties | IFMIF ref |  | ELiTe
Loop surface | 800 m2 |  | 120 m2
Getter | 304 wire mesh |  | 
Volume of mesh | 153 l | 160 l (mesh 40) | 
Capacity for oxygen | 25 kg | 4.2 kg | 
Li flow rate |  | 10 l/min | 
Residence time |  | 10 min | 

## Slide 13: IFMIF nitrogen trap and ELiTe validation
IFMIF reference design uses Ti sponge getter
University of Tokyo develops Fe-Ti getter with 5-10 at.-% Ti to overcome saturation due to formation of TiN layer on pure Ti
Qualification of getter material on laboratory scale by UoT (in stagnant vessel and in small 1 l Li loop)
Main source term is
  Initial Li impurity
  Surface coverage of initial loop surface (1 g/m2)  same assumption as for O
  Recondamination of surfaces and Li during maintenance
13
IFMIF
Properties | IFMIF ref | ELiTe
Getter | Ti sponge | Fe-5% Ti pebbles 0.16 mm diam.
Operating temp. | 580-600C | 
Getter mass | 230 kg | 95 kg
Capacity for nitrogen | 45 kg (30% margin) | 4.2 kg
Li flow rate |  | 10 l/min
Residence time |  | 10 min
ELiTe

## Slide 14: Development and qualification of N getter material
Setup for membrane qualification
University of Tokyo loop for nitrogen trapping

## Slide 15: IFMIF hydrogen trap and ELiTe validation
IFMIF reference design uses Yttrium sponge
Kyushu University develops Yttrium getter based on pebbles saturation
Qualification of getter material on laboratory scale by KU (in stagnant vessels and a small flowing device)
Initial activation of Yttrium surface using HF is important
Cross contamination needs to be avoided
Main source term is
  Deuterium from neutron beam and reaction products of Li-d and Li-n interaction
  D:H:T is 100:6:3
15
IFMIF
Properties | IFMIF ref |  | ELiTe
Getter | Yttrium sponge |  | Yttrium pebbles, 1 mm diameter
Operating temp. | 280-300C |  | 
Getter mass | 70 kg | 25 kg | 
Capacity for H | 3 kg | 1.2 kg | 
Li flow rate |  | 10 l/min | 
Residence time |  | 10 min | 
ELiTe
Hydrogen permeator

## Slide 16: Development and qualification of H getter material
Kyushu University flowing device for hydrogen trapping

## Slide 17: ELiTe safety measures to control spill and fire
ELiTe loop safety approach is based on the rules established for operation of large Na loops in the JAEA Na lab at Oarai
  Rules have been extended to Li operation, but specifity of Li needs to be considered (e.g. reactivity, operating temperature range, weight and specific heat, toxicity, etc.)
  Safety measures have been widely copied in order to facilitate licensing
Detection and control of spills by
  Leak detection wires placed along the piping an all welds placed in the surfaces below the thermal insulation
  Leak detectors on valve stems
  Segmented catch pans (5 m2) with drain pipes to a storage vessel
  Video-sureillance of platform
  Emergency draining of loop

## Slide 18: ELiTe safety measures to control spill and fire
Detection and control of fires
  Smoke detectors
  Ar flooding of air ducts and vessels
  Human intervention to extinguish fires with specific agent NATREX-L (protective clothing and independent air supply)
Containement vessel for target assembly
  Operation under Ar atmosphere
The loop itself is exposed to air
  Li fire in case of spills can thus not be excluded
  Assessment of possible leakages based on accident scenarios

## Slide 19: Qualification of fire extinguishant
Natrex-L (mostly NaCl) has been selected
Coverage with several cm of extinguishant is required to suppress flames and cause drop of pool temperature
The fire-extinguishing behavior of lithium by application of Natrex-L
The fire-extinguishing behavior of dry sand applied to lithium

## Slide 20: IFMIF safety measures
The main requirement for IFMIF is to safely contain the radioactive inventory and do not exceed the legal release limits under normal or any accident situation
Additional measures are therefore required
The rooms (about 1500 m3) containing the Li loop are conceived as a containment, flooded with Ar and kept under a pressure slightly lower than the surrounding rooms
The Ar is conditioned such that a fire cannot develop in case of a leak (minimum air content, low humidity)
The Ar atmosphere needs to be conditioned, since
  Air ingress cannot be excluded
  Tritium diffuses through the loop piping (about 1 MBq/h)
 Recycling of Ar after extraction of the air and of the tritium
20

## Slide 21: IFMIF safety measures
21
Matsushiro et al., Fusion Science and Technology 2005

## Slide 22: Summary and conclusions
Engineering design and validation tasks are closely linked
The proof of principle that stable flow and low impurity levels can be achieved would be an important step forward, but many other issues which may affect operability, performance and costs still have to be resolved until construction
Unfortunately we run out of time in the project which needs to be completed by 2013
22