## Slide 1: Overview of recent progress on plasma current start-up and long-duration plasma maintenance in QUEST
Kazuaki Hanada1, Hiroshi Idei1, Naoaki Yoshida1, Makoto Hasegawa1, Kazuo Nakamura1, Hideki Zushi1, Akihide Fujisawa1, Yoshihiko Nagashima1, Takumi Onchi1, Kengo Kuroda1, O. Watanabe1, Shoji Kawasaki1, Aki Higashijima1, Takahiro Nagata1, Shun Shimabukuro1, Atsushi Fukuyama2, Osamu Mitarai3, Yuichi Takase4, Roger Raman5, and Masayuki Ono6.
1 Research Institute for Applied Mechanics, Kyushu University, Kasuga 816-8580, Japan: 2 Kyoto University, Japan: 3 Tokai University, Japan: 4 The University of Tokyo, Japan: 5 The University of Washington, USA: 6 Princeton Plasma Physics Laboratory, USA
Acknowledgement：
K. Mishraa, h T. Kariyab, M. Yunokia, S. Kojimaa, A. Ejiric, N. Matsumotoc, T.I. Tsujimurad, S. Kubod, H. Ohwadaa, K. Yamasakie, R. Yonedaa, G. Taylorg, N. Bertellig , T. Hondaa,
Z. Wanga, A. Kuzmind, I. Takagif, T. Hirataf, Y. Oyai, M. Miyamotoj , K.Tokunagae
e IGES., Kyushu University : b PRC, University of Tsukuba, : C Univ. of Tokyo, d NIFS : a RIAM, Kyushu University,
f Kyoto Univ. : g PPPL, USA: h IPR, India

## Slide 2: Outline
Introduction of QUEST
Introduction of 28GHz RF system
Recent progress on RF non-inductive plasma current start-up
Recent progress on coaxial helicity injection (CHI) for plasma start-up
Plasma control for steady state operation (SSO)
Recent progress on particle balance research
Summary

## Slide 3: Introduction of QUEST
Height : ～6.6 m
Width : 5 m
Vessel Radius : 1.4 m
Vessel Height : 2.8 m
Vessel Volume: 13.5m3
Toroidal field: <0.25T@0.64m
QUEST (Q-shu University Experiment with Steady-State Spherical Tokamak)
Plasma heating source
2.45GHz : <50kW, CW
8.2GHz : <200kW, CW
8.56GHz : <250kW, CW in preparation
28GHz : <400kW, several sec
OH : 0.2 Vs unipolar operation

## Slide 4: The 28GHz Gyrotron has been Developed in Tsukuba Univ.
28 GHz gyrotron has been developed for Gamma-10/PDX projects at Tsukuba
University.
28GHz 1MW 1s Gyrotorn for PRC(Tsukuba)
Frequency 28GHz Output Power 1MW Pulse Width 1s Output Efficiency 35% (W/O CPD) Beam Voltage 80kV Beam Current 40A MIG triode Cavity Oscillation mode TE8,3 Built-in Mode Converter with Output mode Gaussian like Output Window Sapphire Single Disk Aperture diameter 112mm Collector W/O CPD Sweeping coils
Design Parameters
From T. Kariya
Kyushu Univ. HVPS
75 kV / 25 A =>
max. 0.4 MW
Commercial PS
+
MOSFET SW.
Va

## Slide 5: New Transmission Line (collaborated with NIFS and Tsukuba University)
QO Polarizer System
WG Switch
DL
Double
Disk Window
TMP
TMP
Gyrotron
For CW Operation
Arc Sensors
Viton
O-ring
SS pipe
Water
λ/8
polarizer
λ/4
polarizer
Ti02 Coating
Absorber
2.5-inch CC WG
with Water-cooling Jacket

## Slide 6: Beam Focusing could be checked in a cold test.
Full Wave
Simulation
The irradiant HE11 beam was converted to Gaussian
beam and expanded at the 1st mirror. The mirror
was designed on the phase surfaces to be matched
between the incident HE11 and output Gaussian
beams using a developed Kirchhoff integral code.
The 2nd large mirror sharply focused the expanded
Gaussian beam to a narrow beam with a 5-cm waist
size at the ECR layer.
Full wave simulation
at the ECR layer for
a launching beam
from a 2.5-inch CC WG.
Low power
test results

## Slide 7: Beam Steering could be demonstrated.
Full Wave
Simulation
1st Convex Mirror
2nd Focusing
Mirror
The beam can be steered mainly in the
toroidal direction to have the refractive
parallel index N// from 0 to 1.
Low power
test results
CC WG

## Slide 8: Summary of 2017 Spring/Summer Campaign
#35682 86.4kA
3600sec ＥＣＲ
ＥＣＲ
Pulse duration
Plasma current

## Slide 9: Present Operation regime and target in QUEST
Target

## Slide 10: Visible camera image of Ip Ramp-up Exp. with the 28GHz ECH
28 GHz 250 kW

## Slide 11: Plasma current rapidly increased with HX connts of more than 40keV
PF26:0.59kA
PF352:0.22kA
PF4(1-2A-3-CC1):1.3kA
Ip=-15kA
Transition

## Slide 12: HX measurement indicates presence of energetic electons during current ramp-up.
QUEST
TOP VIEW
28GHzRF 2nd
Resonance layer
(R ≈ 320 mm)
Detector (CdTe)
Ip
e-
FWD
BWD

## Slide 13: Making an strong gas puff from the center stack prevented from plasma current start up.
Gas puff

## Slide 14: Injected RF is much easier to couple with higher temperature electron around 2nd harmonic ECR. But single path absorption cannot be expected.
Calculated results by ＧＥＮＲＡＹ
Ｘ mode oblique injection N//~0.8
Calculated single path absorption is approximately proportional to electron temperature and density when the Ray trajectory of 28GHz does not inflect.
We assume Bulk: 1×1018 m-3, 10eV
Tail: 1×1016 m-3, 100keV.
Density 10-2; Temperature 104 leads to 102 absorption.
When the energetic electron is present in the target plasma, injected RF is likely to deposit on energetic electrons even in the multi-reflection dominant condition.
The first path absorption of 17 % can be expected, when density is 1 x 1017m-3.
The first path absorption is almost proportional to Te.
The first path absorption is almost proportional to ne except near cut-off density (3 x 1018m-3).

## Slide 15: Spike of Ip prevented from increasing Ip
28
8.2
3.09 s
3.09 s

## Slide 16: Progress of CHI experiment project in QUEST
PF3-1
PF5-1
PF3-2
PF5-2
PF2
PF6
PF1
PF7
Ground
(Conducted to vessel)
CHI
Gas injector
− Capacitor +
Bank
QUEST
CHI Capacitor Bank Power supply
CHI Bias
Electrode
Lower
End-plate
CHI Ground
Electrode
Cramic
Break
CHI electrodes
Bias
(Isolated to vessel)
CHI
Electrodes
Result of first CHI experiment
Introduced CHI systems
0
1
2
0
-0.4
-0.8
-1.2
-1.6
-2.0
-2.4
3
50
40
30
20
10
0
-10
[kV]
[kA]
[ms]
Electrode voltage
Injector current
Toroidal current

## Slide 17: Progress of CHI experiment project in QUEST
2.
3.
4.
・In the PF configuration of the picture 2
The plasma evolved up to the top wall and the toroidal current increased up to 48kA.
However, this configuration is not suitable for attaining flux closure.
・In the PF configurations of the picture 3 and 4
In picture 3, current path is to the outer anode plate as expected.
As toroidal current increases, the discharge appears to contact the upper wall plates,
as shown in picture 4.
Improved diagnostics, vertical field control, and performance of capacitor bank to be implemented in future to improve plasma evolution.

## Slide 18: Plan of high field side injection of 8.2GHz for EBW plasma current start-up to make higher density plasma
Presented by Mr. Hatem in this conference

## Slide 19: Main target of SSO on QUEST is particle balance
MHD
E. conf
Cur. Diff.
Part + Imp
Retention
Erosion/deposition
10-3 | 10-2 | 10-1 | 1 | 101 | 102 | 103 | 104 | 105
Heat loads
[s]
Tokamaks operating long pulses have to overcome and control several plasma-core and plasma-wall interaction time scales
ITER pulses
400s – 3000s
JET
10s
QUEST
2h14m
JT-60SA
100s
TRIAM-1M
5h16m
LHD
48m

## Slide 20: Recent progress on SSO in QUEST
Hot wall since 2015
SSO is the most important issue to realize fusion power plant. Particle balance including tritium retention is crucial, but few experiments were executed.

## Slide 21: Particle fueling feed-back control for SSO
Fig. 5. Gas fueling control with monitoring Ha. (a) Ha signal filtered by a digital low-pass filter (solid line) and raw signal (dashed line), (b) Ha signal widened by time and the voltage applied to the piezo valve.
Piezo valve control by changing the duty of repetitive gas puff.
M. Hasegawa, et al., Fusion Engineering and Design, 112 (2016) 699-702
Mass flow control by changing the flow rate of fueling with PID loop
--- Two types of actuators can be used for feed-back control referring to Ha signal. ---
Maximum fueling rate
Gas puff:
qfuel = 2.0×1021 Hs-1
Mass-flow:
qfuel = 1.7×1019 Hs-1
Ha signal is kept at the target value
by decreasing the flow rate gradually.
Total H Flux to the wall is expected to be proportional to Ha signal level.
When Ha level is kept constant, change of wall pumping rate must be caused by net emission of H2.

## Slide 22: Plasma discharge of 1hour 55min
H2 pressure (Pa)
Ha (a.u.)
H2 flux (ml/min)
Iphall (kA)
0
2000
4000
6000
Time (sec)
Gas fueling is feed-back controlled with mass flow controller to keep Ha constant.
Temperatures of hot wall and vessel wall are kept 120℃ constant.
Plasma current is measured with hall sensors.
Fueling rate is decreased gradually to keep Ha constant, and it finally become zero.
After that, Ha increases gradually, and finally plasma discharge is terminated spontaneously.
Phase I
Phase III
Phase II

## Slide 23: Investigation of Plasma facing wall with TEM, Ellipsomerty and Colormetry
Photo of inner vessel and specimen for TEM and Ellipsometry before installation of the hot wall
Component and thickness of plasma-induced thin film on the surface
Thickness distribution
Top
Bottom
100nm
Published to RSI, Z.Wang et al.

## Slide 24: A wall model with hydrogen barrier (HB) is proposed
Advanced Fusion Research Center
26th IAEA Fusion Energy Conference, EX/P4-49, K. Hanada, et. al.
To be published in Nuclear Fusion, K.Hanada, et. al.
:the number of H dissolved in wall material
:the number of H trapped in defects
:the upper-limit number of
:net influx per unit area into wall material
: surface area
: surface recombination coefficient of H atoms
: thickness of deposition layer
: H trapping rate
: H de-trapping rate
In this model, H atoms don’t move from deposition layer to SUS substrate and vice versa due to high chemical potential.
Hw and HT are total numbers of H atoms in deposition layer.
Release due to recombination
Influx to the deposition layer
Trapping
De-trapping
Distance from wall surface

## Slide 25: Comparison between experimental results and HB model
 | Wall pumping rate (H/sec) | Wall stored H
HB model |  | (=0 @t=0)
Experimental |  | 
 | Wall pumping rate (H/sec) | Wall stored H
HB model |  | 
Experimental |  | 
Wall stored H
Wall pumping (H2/s)
Phase I
Phase II
Phase III
CX
Ionization
Total
HB model
The wall-stored H gradually increase with the decrease of wall pumping rate.
In phase III, wall release starts with the decrease of wall stored H.

## Slide 26: Hot wall can modify wall pumping rate and H recycling rate

## Slide 27: Future Plans
Hot wall + water cooling
CW 28 GHz system
SSO of more than 100kA plasmas

## Slide 28: Summary
The plasma current start-up without fundamental ECR could be demonstrated by 28 GHz microwave injection on QUEST. The plasma current up to 86 kA could be achieved with 250kW injection (0.35A/W) which is in large part responsible for the improvement of transmission line.
Coaxial helicity injection has been executed and reliable plasma breakdown could be observed. Toroidal current of up to 48 kA could be achieved, but closed flux surface was formed.
High field Injection of 8.2 GHz is planning to excite EBW effectively.
Feedback control of Ha is effective to achieve long duration discharge and three phases of particle balance could be observed.
Plasma-induced film on the surface of plasma facing wall has been investigated and the film Plays an essential role in particle balance.
Hydrogen barrier model is proposed to explain the progress on particle balance in the long duration discharge. In phase I and II, the model could express the progression.
The Hot wall has the possibility to control the wall pumping and the hydrogen recycling.

## Slide 30: HB model agrees well with experimental results, excluding Phase III.
The wall-stored H gradually increase with the decrease of wall pumping rate.
In phase III, wall release starts with the decrease of wall stored H.
The number of trapped particles is saturated with longer time constant.
Wall stored H
Wall pumping (H2/s)
Phase I
Phase II
Phase III
HB model

## Slide 31: Comparison between experimental results and HB model
 | Wall pumping rate (H/sec) | Wall stored H
HB model |  | (=0 @t=0)
Experimental |  | 
 | Wall pumping rate (H/sec) | Wall stored H
HB model |  | 
Experimental |  | 
Wall stored H
Wall pumping (H2/s)
Phase I
Phase II
Phase III
CX
Ionization
Total
Total H Flux to the wall is expected to be proportional to Ha signal level.
When Ha level is kept constant, change of wall pumping rate must be caused by net emission of H2.
HB model

## Slide 32: Incident polarization scan indicates single path absorption was dominant.
Incident Polarization Scanning
High non-inductive Ip of 70 kA has been
achieved using a new 28 GHz launcher.

## Slide 33: The same operation of human-conducted control gave rise to complete different plasma start-up. The plasma start-up was quite sensitive to hydrogen recycling from the center stack.
Standard operation
After strong gas puff

## Slide 34: 2nd ECR 28GHz Plasma start-up(#35713)（九大提供）

## Slide 35: Transition from bulk heating to tail heating was observed in the early phase of plasma start-up. （九大、東大提供）
Rapid Ip ramp-up was observed.
Bulk electron temperature was significantly reduced from 100 eV to 5 eV.
Electron density of 1 x 1018 m-3 was not so different.
AXUV and Ha signals were significantly reduced.
XUV with an aluminum filter of 0.4 mm in thickness signal did not become altered so much.
HXR signals beyond 40keV was enhanced.
After the transition

## Slide 36: TS Diagnostics（東大提供）
HX
2nd ECR
for 28 GHz
2nd ECR
for 28 GHz
1st ECR
for 8,2 GHz
1st ECR
for 8,2 GHz
Before the HX built-up,
Te peaks were observed near
the ECR layers, while Te deceased
after the HX built-up.
The plasma current was ramped up
with the HX built-up.
t = 2.4 s
t = 2.9 s
t = 3.3 s

## Slide 37: Resonance condition at high field side of 2nd ECR layer is satisfied by bi-directional drifting electrons, but …
Energy=25, 50, 100keV
Pperp/mc
Ppara/mc
keV
Pitch Angle
2nd ECR R=0.32m
LFS of 2nd ECR
1m
CNT direction of
Plasma current
Co direction of
Plasma current
A
N//=0.78
R=0.35m
Resonance curve
B
A
B
Area is wide.
A
B
C

## Slide 38
Resonance condition in the low field side is satisfied by only CNT drifting electrons, when single path absorption is dominant. It is expected to make a current drive originally intended.
Energy=25, 50, 100keV
Pperp/mc
Ppara/mc
keV
Pitch Angle
2nd ECR R=0.32m
LFS of 2nd ECR
1m
CNT direction of
Plasma current
Co direction of
Plasma current
A
N//=0.78
R=0.35m
Resonance curve
B
A
B
Area is wide.
Drifting CNT-direction
Drifting CNT-direction
B
A

## Slide 39: Injected RF is much easier to couple with higher temperature electron around 2nd harmonic ECR. But single path absorption cannot be expected.
Calculated results by ＧＥＮＲＡＹ
Ｘ mode oblique injection N//~0.8
Calculated single path absorption is approximately proportional to electron temperature and density when the Ray trajectory of 28GHz does not inflect.
We assume Bulk: 1×1018 m-3, 10eV
Tail: 1×1016 m-3, 100keV.
Density 10-2; Temperature 104 leads to 102 absorption.
When the energetic electron is present in the target plasma, injected RF is likely to deposit on energetic electrons even in the multi-reflection dominant condition.
The first path absorption of 17 % can be expected, when density is 1 x 1017m-3.
The first path absorption is almost proportional to Te.
The first path absorption is almost proportional to ne except near cut-off density (3 x 1018m-3).

## Slide 40: Equilibrium calculation also indicates the plasma shrinking before the transition.
PF26:0.59kA
PF352:0.22kA
PF4(1-2A-3-CC1):1.3kA
Ip=-15kA
Transition

## Slide 41: Plasma was shrinking before transition and detached from the center stack. It is expected to produce less PWI and reduce hydrogen emission from the wall.
142
151
154
155
156
157

## Slide 42: Modelling of the transition with estimation of Life time of energetic electron
3keV
10keV
50keV
QUEST@R=0.64m
200ms
100ms
100ms
Ip (kA)
te
te
te
Ip (kA)
When the plasma is shrinking into high field side, t// is constant. The collision time between neutral with energetic electron is approximately several 10 mm [1]. Therefore the collision may prevent from production of energetic electrons.
[1] D.Sengupta, et al. Pramana, 11, 661 (1978)
Collision time
Ip (kA)
Ip (kA)

## Slide 43: 2nd Transmission Line for Local ECHCD (NIFS及び九大提供）
λ/8
polarizer
λ/4
polarizer
Launcher
with a
focusing
mirror
X-mode Injection
for 2nd ECHCD
Polarization control to
excite X-mode in the
oblique injection
Beam focusing to obtain
a narrow beam

## Slide 44: W-Be壁の導入により静的吸蔵から動的吸蔵へ
JET ILW
W-Be壁(ILW)の導入により放電終了時の重水素放出が促進されて、トリチウムの長期吸蔵による放射化レベルは激減した。一方放電中の重水素放出（動的吸蔵）の影響はより顕著になった。
V. Philipps et al, J. Nucl. Matr. 438 (2013) S1067–1071
S. Brezinsek et al Nucl. Fusion 53 (2013) 083023

## Slide 45: The same operation of human-conducted control gave rise to complete different plasma start-up. The plasma start-up was quite sensitive to hydrogen recycling from the center stack.
Standard operation
After strong gas puff

## Slide 46: Making an strong gas puff from the center stack prevented from plasma current start up.
Gas puff

## Slide 47: Modelling of the transition with estimation of Life time of energetic electron
3keV
10keV
50keV
QUEST@R=0.64m
200ms
100ms
100ms
Ip (kA)
te
te
te
Ip (kA)
When the plasma is shrinking into high field side, t// is constant. The collision time between neutral with energetic electron is approximately several 10 mm [1]. Therefore the collision may prevent from production of energetic electrons.
[1] D.Sengupta, et al. Pramana, 11, 661 (1978)
Collision time
Ip (kA)
Ip (kA)

## Slide 48: Plasma was shrinking before transition and detached from the center stack. It is expected to produce less PWI and reduce hydrogen emission from the wall.
142
151
154
155
156
157

## Slide 49: Equilibrium calculation also indicates the plasma shrinking before the transition.
PF26:0.59kA
PF352:0.22kA
PF4(1-2A-3-CC1):1.3kA
Ip=-15kA
Transition

## Slide 50: Incident polarization scan indicates single path absorption was dominant.
Incident Polarization Scanning
High non-inductive Ip of 70 kA has been
achieved using a new 28 GHz launcher.

## Slide 51: 3rd Transmission Line （筑波大学、NIFS、九大提供）
QO Polarizer System
WG Switch
DL
Double
Disk Window
TMP
TMP
Gyrotron
For CW Operation
For CW Operation
Arc Sensors
2.5-inch CC WG
with Water-cooling Jacket
Viton
O-ring
Viton
O-ring
SS pipe
Water

## Slide 52: Beam Steering（九大提供）
Full Wave
Simulation
1st Convex Mirror
2nd Focusing
Mirror
The beam can be steered mainly in the
toroidal direction to have the refractive
parallel index N// from 0 to 1.
Low power
test results
CC WG

## Slide 53: Beam Focusing（九大提供）
Full Wave
Simulation
The irradiant HE11 beam was converted to Gaussian
beam and expanded at the 1st mirror. The mirror
was designed on the phase surfaces to be matched
between the incident HE11 and output Gaussian
beams using a developed Kirchhoff integral code.
The 2nd large mirror sharply focused the expanded
Gaussian beam to a narrow beam with a 5-cm waist
size at the ECR layer.
Full wave simulation
at the ECR layer for
a launching beam
from a 2.5-inch CC WG.
Low power
test results

## Slide 54: Heater of the hot wall was off during long duration discharge
Total heater powers to keep 120 ℃ without plasma are about 5 kW in vessel wall, and less 1 kW in hot wall.
Temperatures of most parts increase up in the same way due to the plasma radiation.
Heater power of hot wall becomes zero because of the increase of hot wall temperature.
Heater power of vessel wall decreases gradually.
Vessel wall
Hot wall
Jun. 30, 2017
Plasma discharge
with 35 kW RF
Locations of thermocouple

## Slide 55: Cooling function for vacuum vessel wall
Temperature of vacuum vessel has to be kept under 150℃ to protect diagnostics and plasma-heating devices.
Water cooling channels are installed at the ribs of vacuum vessel and vacuum ports.

## Slide 56: Cooling function for hot walls
Sheath heater profile (Red)
3D view of one section HCP
Cross section of heating-cooling channels
High
Low
~50mm
Two water cooling channels are prepared, which are connected to the panel with appropriate SUS316L plates (thickness and distance).
This provides two different thermal resistances to the panel, and the cooling capacity will be adjusted with the combination of cooling channels.
Cooling capacity: H water < L water < H&L water

## Slide 57: HX measurements
QUEST
TOP VIEW
28GHzRF 2nd
Resonance layer
(R ≈ 320 mm)
Detector (CdTe)
Ip
e-
FWD
BWD

## Slide 58: Fast camera images at Ip drop
28
8.2
3.09 s
3.09 s