Culham Future Devices Under Study

Garry Voss

Outline

(	ST Power Plant

(	Machine Layout

(	Neutronic Analysis

(	Centre Column Design

(	Breeder Blanket Design

(	Divertor concept

(	Maintenance

(	Power Cycles

(	Burning ST

Advantages of the ST

| ( Low aspect ratio (A) allows operation at high beta. ( Low A offers stability at high elongation providing a route to high bootstrap current fraction and uniform neutron wall load. ( ST offers resilience to disruptions. ( No inboard blanket and a single turn TF coil allows simple maintenance. |  |
| --- | --- |

Machine Layout

Neutronic Analysis

(	       MCNP code used for Neutronic analysis

(	    TBR = 1.16

Centre Column Design

Thermo-hydraulic Analysis of Centre Rod

|  | Cooling fraction = 15% Water velocity = 10 m/sec Pressure drop = 12 bar Total heat load in rod = 242 MW 158 MW electrical 84 MW nuclear |
| --- | --- |

Nuclear Effects in the Centre Rod

| dpa v. Radius at Mid-plane | Nuclear Heating rate v. Radius at Mid-plane |
| --- | --- |

Neutron heating in rod = 84 MW

Neutron heating in shield = 244MW

Electrical power in rod = 158 MW

Power Cycles

Steam cycle efficiency = 42%       Net power generated = 1250 MW

Blanket Design & Construction

| ( Helium cooled pebble bed blanket technology ( Lithium silicate with beryllium multiplier. ( Corrugated steel panel structure between gas cooled plates. ( Tubular 1st wall cooled by internal vortex flow regime. ( Blanket composition: Li4 Si04 16% Be 64% Steel (F82H) 12% Helium (80bar) 8% ( 16 equitorial blanket modules 32 polar blanket modules. ( Thickness of Li4 Si04 bed 4.5mm Thickness of multiplier bed 9mm |  |
| --- | --- |

Blanket Optimisation

| Heat Generation Rate profiles | Helium gas temperature profiles |
| --- | --- |

( Max. temperature in the Li4SiO4			645(C

( Max. temperature in the multiplier		620(C

( Max. 1st wall temperature 				580(C

( Max. cooling plate temperature			600(C

Divertor Concept

| ( Scheme design of a cascading pebble divertor system is currently in progress. ( A curtain of SiC balls 3mm in diameter fall across divertor legs. ( A pneumatic conveyor is used to return pebbles to the top. ( Heat is extracted from the transport gas. |  |
| --- | --- |

Maintenance

( Centre column and blanket modules are

removed/replaced from beneath the power core.

( Target for Availability ( 80%

##### Burning Spherical Tokamak

| Aspect ratio 1.5 Major radius 1.75m Minor radius 1.17m Elongation 3.0 Triangularity 0.6 Plasma current 17MA Rod current 20MA Normalised beta (N 4.0 Fusion power 324MW NBI Power 27MW Q 11.9 HIPB98(y,1) 1.23 Bootstrap current fraction 0.48 |  |
| --- | --- |

Evolution of Burning ST Parameters

| Parameter | START (32993 | MAST (2948 | Burning ST Aug 2000 | Burning ST March 2001 | Burning ST May 2001 | Burning ST Aug 2001 | ST Power plant |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Aspect ratio | 1.38 | 1.37 | 1.5 | 1.5 | 1.5 | 1.5 | 1.4 |
| Elongation( | 1.8 | 1.9 | 2.2 | 2.2 | 3.0 | 3.0 | 3.2 |
| Triangularity | 0.6 | 0.45 | 0.3 | 0.3 | 0.6 | 0.6 | 0.5 |
| Norm. beta (N | 4.2 | 3.1 | 3.2 | ~5 | 3.7 | 4.0 | 8.2 |
| HIPB98(y,1) | >1 | ~1.2 | 1.2 | ~1.5 | 1.5 | 1.23 | 1.2 |
| Plasma current MA | ~0.25 | 0.55 | 20 | 16 | 17 | 17 | 31 |
| Major radius m | 0.32 | 0.74 | 2.4 | 2.4 | 1.75 | 1.75 | 3.4 |
| Minor radius m | 0.23 | 0.54 | 1.6 | 1.6 | 1.17 | 1.17 | 2.4 |
| Solenoid flux swing | 0.08Vs | 1Vs | 20Vs | 23Vs | 10.5Vs | 9.0Vs | ---- |
| Irod/Ip | ~1 | ~3 | 0.9 | 0.9 | 1.27 | 1.18 | 1 |
| Q | --- | ---- | 10 | 10 | 10 | 12 | ~50 |

Centre Rod Insulation Strength Testing

The shear strength of glass/epoxy insulation between centre rod conductors is accurately represented by the torsion test specimen below.

The flared ends reduce shear stress at the ends giving a uniform high stress (no stress concentrations) over the central section. Stainless steel end crowns potted into the structure eliminate end effects

Three test samples will be tested to determine:

room temperature and high temperature static strength, and high temp.fatigue.