13_031105_CLN_01.doc

TO: DISTRIBUTION

FROM: C NEUMEYER

SUBJECT: TF TORQUE COLLAR WET LAY-UP SHEAR STRENGTH

The following table shows the E120-HP wet lay-up shear data including the final results from group 6 (G6).

|  | Normal Stress (psi) | Shear Failure Stress (psi) |
| --- | --- | --- |
| G4 | 232 | 2876 |
| G4 | 240 | 2921 |
| G4 | 287 | 2521 |
| G5 | 301 | 3037 |
| G5 | 363 | 2651 |
| G5 | 994 | 3946 |
| G5 | 1002 | 4429 |
| G6-1 | 1018 | 2935 |
| G6-2 | 1018 | 3610 |
| G6-12 | 1125 | 3220 |
| G5 | 1999 | 5191 |
| G5 | 2004 | 5069 |
| G6-4 | 2036 | 4104 |
| G6-3 | 2075 | 3632 |
| G6-5 | 3131 | 4259 |
| G6-11 | 3878 | 4244 |
| G6-7 | 4099 | 4398 |
| G6-6 | 4114 | 4629 |
| G6-8 | 5011 | 4223 |
| G6-10 | 5365 | 4881 |
| G6-9 | 5438 | 4251 |

A fit was made to the minimum of the data, and then a peak equivalent to that fit based on the 1.08 peak-to-average applied to the zero compression value. This result is shown superimposed, along with the prior assumption. The equation for the peak fit is…

For compression <= 3000 psi….

Shear Stress = 1.08*2300+0.625*Compression

For compression > 3000 psi….

Shear Stress = 1.08*2300+0.625*3000

…where shear and compression are in psi.

Safety factor calculations shall be based on the peak fit curve as shown.

Cc:

P Heitzenroeder	C Jun		M Kalish	T Kozub	I Zatz

-----Original Message-----
From: Chang H. Jun [mailto:cjun@pppl.gov] 
Sent: Tuesday, September 30, 2003 11:34 AM
To: 'cneumeyer@pppl.gov'; 'pheitzen@pppl.gov'; 'izatz@pppl.gov'; 'mkalish@pppl.gov'
Subject: [NSTX] About maximum shear ratio of 1.65 


Gentlemen,


The E value of Hysol was measured by two compression test at PPPL.

The test results show very low E value.

The measured value is less than 0.1Mpsi (normal Epoxy is ~1.5Mpsi) 

Because of this low E of Hysol material, maximum shear ratio of 1.65 is no longer valid.

I tested it by FEA analysis with 0.5MN on the 9.5cm*8.3cm*2 areas of shear plane.

Average shear is 500,000/(0.095*0.083*2) = 31.7MPa

********************************************************************************************
                              E of 1Mpsi (I used before)                      E of 0.1Mpsi
********************************************************************************************
Max shear stress=         51.3MPa    (162%)                                34MPa    (108%)
********************************************************************************************

So, now new ratio is barely 1.08 or less than 1.1, instead of 1.65.

This is caused by the softness of the material. That means the stresses spread more widely in more soft material.

If you need more verification, please let me know it.


Thanks,   Chang

# Footnotes

Data supplied by T Kozub, see final test report

E-mail from C. Jun, 9/30/3 (attached)