13_031113_CLN_01.doc

TO: DISTRIBUTION

FROM: C NEUMEYER

SUBJECT: TF TORQUE COLLAR WET LAY-UP SHEAR STRENGTH, REVISED

This memo supercedes a prior one (13_031113_CLN_01.doc ) on the same subject, based on revised values of modulus measured for the wet lay-up, and calculated peak/average ratio of the test samples.

The following table shows the E120-HP wet lay-up shear data including the final results from group 6 (G6).

|  | Normal Stress (psi) | Shear Failure Stress (psi) |
| --- | --- | --- |
| G4 | 232 | 2876 |
| G4 | 240 | 2921 |
| G4 | 287 | 2521 |
| G5 | 301 | 3037 |
| G5 | 363 | 2651 |
| G5 | 994 | 3946 |
| G5 | 1002 | 4429 |
| G6-1 | 1018 | 2935 |
| G6-2 | 1018 | 3610 |
| G6-12 | 1125 | 3220 |
| G5 | 1999 | 5191 |
| G5 | 2004 | 5069 |
| G6-4 | 2036 | 4104 |
| G6-3 | 2075 | 3632 |
| G6-5 | 3131 | 4259 |
| G6-11 | 3878 | 4244 |
| G6-7 | 4099 | 4398 |
| G6-6 | 4114 | 4629 |
| G6-8 | 5011 | 4223 |
| G6-10 | 5365 | 4881 |
| G6-9 | 5438 | 4251 |

A fit was made to the minimum of the data, and then a peak equivalent to that fit based on the 1.2 peak-to-average applied to the zero compression value. This result is shown superimposed, along with the prior assumption. The equation for the peak fit is…

For compression <= 3000 psi….

Shear Stress = 1.2*2300+0.625*|Compression| = 2760+0.625*|Compression|

For compression > 3000 psi….

Shear Stress = 1.2*2300+0.625*3000 = 4635

…where shear and compression are in psi.

Safety factor calculations shall be based on the peak fit curve as shown.

Cc:	P Heitzenroeder	C Jun		M Kalish	T Kozub	I Zatz

# Footnotes

Data supplied by T Kozub, see final test report

E-mail from C. Jun, 11/13/3