National Spherical Torus Experiment

NSTX

SPECIFICATION

FOR

OH and PF Copper Conductors

NSTX-SPEC-13-037

Revision 0

3/27/97

PREPARED BY:_____________________________

J Spitzer

APPROVED BY:_____________________________

P Heitzenroeder

PRINCETON UNIVERSITY

PLASMA PHYSICS LABORATORY

(PPPL)

P.O. BOX 451

PRINCETON, N.J. 08543

| Revision | Date | TRB | Description of Change |
| --- | --- | --- | --- |

| 0 | 3/27/97 |  | Initial Release |
| --- | --- | --- | --- |

1.0 SCOPE	1

2.0 APPLICABLE DOCUMENTS	1

2.1 Conductor Drawings	1

2.2 Standards and Codes	1

3.0 REQUIREMENTS	2

3.1 Material	2

3.2 Strength	2

3.3 Electrical Conductivity	2

3.4 Shapes	2

3.5 Quantities and Lengths	3

3.6 Identification and Marking	3

4.0 TEST REQUIREMENTS	3

4.1 Billets	3

4.1.1 General Inspection	3

4.1.2 Microscopic Examination	3

4.1.3 Embrittlement	4

4.2 Extruded Conductors	4

4.2.1 General Inspection	4

4.2.2 Dimensional Measurements	4

4.2.3 Measurement of Properties	4

5.0 QUALITY ASSURANCE REQUIREMENTS	5

5.1 Inspection/ Surveillance/Audit By Princeton	5

5.2 Subcontractor's Responsibility For Conformance	5

5.3 Subcontractor Quality Assurance Program	5

5.4 Quality Assurance Plan	6

5.5 Manufacturing/ Inspection/Test Plan	6

5.6 Inspection And Test Procedures	6

5.7 Document Traceability And Records	6

5.8 Equipment/Material Identification And Status	6

5.9 Document Review, Approval And Control	6

5.10 Calibration Of Test And Measuring Equipment	7

5.11 Release For Shipment Form	7

5.12 Process History	7

5.12.1 Certificate Of Compliance (CofC)	7

5.12.2 Material Certifications	7

5.12.3 Manufacturing/Inspection/Test Documents	7

5.12.4 Inspection Reports	7

5.12.5 Test Reports	7

5.13 PPPL RECEIVING/ INSPECTION	8

6.0 DOCUMENTATION REQUIREMENTS	8

6.1 Proposal Technical Documentation	8

6.2 Documentation After Contract Award and Prior to Fabrication	8

6.3 Documentation Prior to Shipment	8

7.0 HANDLING, SHIPPING AND STORAGE	8

1.0 SCOPE

a. This specification defines the alloy, form, quantity and integrity of the hollow extruded copper conductors for the National Spherical Torus Experiment (NSTX) Ohmic Heating (OH) coil and the Poloidal Field (PF) Coils 1a and 1b. To minimize the risk of coil failure, for any reason, strict adherence to these specifications and the associated drawings is essential.

b. Seller shall furnish all material, labor  and facilities necessary to complete the work as defined in the contract documents subject to the qualifications, conditions, or exceptions noted.

2.0 APPLICABLE DOCUMENTS

2.1 Conductor Drawings

a. Conductor drawings identified in the Appendix are part of this specification.

b. Dimensions in drawings and specifications shall refer to conditions at room temperature (20 degrees Centigrade).

2.2 Standards and Codes

a. All materials shall comply with the latest revision of the following documents in effect at the date of the approved purchase order.  These documents form a part of this specification to the extent referenced herein.

ASTM Standards

B193	Test for the Resistivity of Electrical Conductor Materials

B577	Test of Hydrogen Embrittlement of Copper

E8	Tension Testing of Metallic Materials

E18	Test for Rockwell Hardness and Rockwell Superficial Hardness of Metallic Materials

B170	Oxygen-Free Electrolytic Copper Wire Bars

B188	Seamless Copper Bus Pipe and Tube

B187	Copper Bus Bar, Rod and Shapes

B353	Chemical Analysis of Copper (Electrolytic Determination of Copper

B342	Electrical Conductivity by Use of Eddy Currents

Copper Development Association

CDA Standards Handbook, Part 2 (Wrought Products) Alloy Data, CDA Alloy No. 10700.

b. The above Standards and Codes set forth the minimum requirements.  They may be exceeded by the Seller with written permission from PPPL, if in the Subcontractor's judgment, superior of more economical designs or materials area available for successful and continuous operations as required by the specification.

c. Seller agrees, represents and warrants that all services, designs and material sold or otherwise provided to PPPL by the Seller comply with applicable Federal, State and Local laws, regulation and codes, and all applicable specifications and standards, including those specified above, in each case is in effect at the date of the order placement.  Seller shall advise PPPL of the codes, standards and requirements complied with in the design and fabrication of the deliverable items.

3.0 REQUIREMENTS

3.1 Material

The material required is CDA No. 10700 oxygen-free copper with silver content of 25 troy oz/ton (.085% Ag).  The material shall be of such quality and purity that the finished product shall have the properties and characteristics prescribed in this specification and shall be cold drawn to produce the required temper, edge and surface finish.  The conductors shall be furnished in the cold drawn condition.

3.2 Strength

a.  Yield Strength shall be 36,000 psi min. to 38,000 psi max. (0.5% elongation)

b. Ultimate Tensile Strength shall be 42,000 psi minimum @ 15% elongation

c. Hardness checks shall be used to verify the uniformity of the properties along the conductor lengths.

3.3 Electrical Conductivity

a. Electrical conductivity shall be 100% minimum IACS.

3.4 Shapes

a. Two shapes are required, one for the OH and one for the PF coils. See drawings listing in the Appendix.

b. Dimensional tolerances are given on the drawings listed in the Appendix.

c. The profile of the cooling hole shall be circular. The hole profile shall show neither re-entrant material or notches greater than 0.020 true measure when viewed at a magnification of 100x. Cracks, laps, fold, scale and any other discontinuity longer than 0.020 inch true length normal to the hole surface, shall not be present a magnification of 100x.

3.5 Quantities and Lengths

a. Required quantities and lengths are listed in the following Table 3.5-1.

b. Lengths listed are continuous extruded lengths.  Brazed joints are not permitted.

c. Total estimated weight (for information only) of conductors to be delivered is 4904 lbs for the OH conductors and 2142 lbs for the PF1 Conductors.

Table 3.5-1: Conductor Quantities and Lengths

Conductor

CSA

Minimum Supplied Length

Est Weight per bar

Quantity

(in^2)

(ft)

(lbs)

OH1

0.2192

319.0+1.0

271.0

4

OH2

0.2192

347.0+1.0

294.8

4

OH3

0.2192

376.0+1.0

319.5

4

OH4

0.2192

401.0+1.0

340.7

4

PF1a

0.5195

214.0+1.0

430.9

3

PF1b

0.5195

211.0+1.0

424.9

2

Notes:

1 - CSA refers to effective copper cross sectional area of the conductor

2 - Supplied length is the required length to be supplied

3 - Estimated weight is for information only

3.6 Identification and Marking

Conductors shall be tagged and marked, and supplied on reels marked with "Conductor"-"Item #", where "Conductor" is the conductor identified in Table 3.5-1 and "Item #" is sequential number ranging from 1 to the quantity to be supplied as listed in Table 3.5-1, e.g. OH1-3 would identify the 3rd piece of the 4 to be supplied of the OH1 type conductor.

4.0 TEST REQUIREMENTS

4.1 Billets

4.1.1 General Inspection

Extrusion billets shall be free of shrink holes, porosity, cracks, cold sets, inclusions, pits, and similar defects. The metal furnished shall be of uniform purity and grade.

4.1.2 Microscopic Examination

The test specimens of the material designated as C10700 shall be free of cuprous oxide as determined by Procedure A of Methods B577.  In the case of a dispute, a referee method, in accordance with Procedure C, shall be employed.

4.1.3 Embrittlement

It is required that the material designated as C10700 pass the embrittlement test as indicated in ASTM B170 Paragraph 7.5 and Procedure B of Methods B577.  In the case of a dispute, a referee method, in accordance with Procedure C, shall be employed.

4.2 Extruded Conductors

4.2.1 General Inspection

The finished material shall be free from blisters, slivers, laps, seams, cracks and scale, as well as from all other imperfections, such as damaged corners or edges, not consistent with best commercial practice, and shall be bright and clean.  Inspection procedures shall be proposed by Subcontractor and approved by PPPL.

4.2.2 Dimensional Measurements

a. Conductors shall be checked to verify that the cross-sectional dimensions are within the required tolerance. Method and number of measurement locations shall be proposed by Subcontractor and approved by PPPL.

b. Conductors straightness shall be per ASTM B187..

c. Conductors shall be checked to verify that the length of each item listed in Table 3.5-1 is within the required tolerance.

d. Conductors shall be checked to verify that the cross section and centering of the cooling hole is within the required tolerance. Method shall be proposed by Subcontractor and approved by PPPL.

4.2.3 Measurement of Properties

a. Each extruded conductor shall be subjected to the Rockwell hardness test as prescribed in ASTM E18.  Measurements shall be taken along the entire length of each extruded conductor at intervals of not less than three feet along the length.  The values for Rockwell hardness shall indicate yield strengths within the range indicated in Section 3.2.  Details of the methodology for conversion of Rockwell hardness to copper yield strength shall be proposed by the Subcontractor prior to testing and approved by PPPL.

b. One sample piece shall be cut from each extrusion for the OH coil and one from each extrusion for the PF1a and PF1b coil for test specimens as described below.  If any test specimen shows defective machining or develops flaws, it may be discarded and another specimen substituted.

b.1. Specimens taken from each sample piece shall be subjected to the electrical resistivity test as prescribed in ASTM B193.

b.2. A 10% random set of specimens shall be taken from the sample lot and tested for yield properties and tensile properties.

b.3. If the percentage elongation of any tension test specimen is less than that specified and any part of the fracture is outside the middle two-thirds of the gage length or in a punched or scribed mark within the reduced section, a retest of an additional specimen, either from the same sample piece or a new sample piece is allowed.

5.0 QUALITY ASSURANCE REQUIREMENTS

5.1 Inspection/ Surveillance/Audit By Princeton

Authorized representatives of PPPL and the U. S. Government shall have the right at all reasonable times to visit the Subcontractor's premises and those of Subcontractor's suppliers during the performance of the procurement for the purposes of inspection, surveillance, audit and/or obtaining any required information as may be necessary to assure that items or services are being furnished in accordance with specified requirements. Such visits shall be coordinated with the Subcontractor's personnel to minimize interference with the normal operations of said premises. The Subcontractor shall make available records and documentation necessary for this function and shall provide all reasonable facilities and assistance for the safety and convenience of PPPL and/or U. S. Government representatives in the performance of their duties.   PPPL and the U. S. Government recognize the Subcontractor's right to withhold information concerning proprietary processes. The Subcontractor agrees to insert the paragraph above in each lower tier procurement issued hereunder.

5.2 Subcontractor's Responsibility For Conformance

Neither PPPL's review and/or approval of Subcontractor's documents nor PPPL's inspection of Subcontractor's items or services shall relieve the Subcontractor of responsibility for full compliance with requirements of the purchase order/contract.

5.3 Subcontractor Quality Assurance Program

The Subcontractor shall have and maintain an effective Quality Assurance Program. The objectives of such a program are to assure that the Subcontractor's work meets the required level of quality and is performed in accordance with contractual requirements.

5.4 Quality Assurance Plan

Subcontractor shall submit as soon as practical after the subcontract/purchase order award, three (3) copies of its Quality Assurance Plan, describing the specific quality assurance and quality control procedures and practices to meet the requirements of this particular subcontract/purchase order, for PPPL review and approval.

5.5 Inspection/Test Plan

Subcontractor shall prepare and submit for PPPL review and approval ten (10) days prior to first article fabrication, two (2) copies of an Inspection/Test Plan which identifies critical inspections and tests. Preparing the Plan may include developing a flow chart and generating Process Sheets/Shop Travelers, etc. PPPL may designate selected inspection and/or test operations as mandatory "witness" points based on the plan.

5.6 Inspection And Test Procedures

Inspections and tests shall be performed in accordance with written procedures referencing criteria for acceptance or rejection.  Adequate records shall be maintained and available for PPPL's review. Procedures for all tests on extruded conductors listed in section 4.2 shall be submitted with the Inspection/Test Plan per section 5.5.

5.7 Document Traceability And Records

The Subcontractor shall maintain a system of documentation whereby objective evidence of required operations, inspections, examinations, and tests is systematically compiled, indexed and stored.  Such objective evidence may include "travelers"; and material test, certification, inspection, examination, test and discrepancy reports; which shall be complete, legible, and validated by responsible personnel and shall be traceable to subject items.

5.8 Equipment/Material Identification And Status

Material and equipment identification shall be maintained throughout the program and be traceable to the records. Status of acceptability shall be readily discernible through the Subcontractor's use of tags, stamps, serial numbers or other positive means.

5.9 Document Review, Approval And Control

The Subcontractor shall provide a system for distribution and control of approved documents and changes thereto. The system shall use procedures which provide for review and approval of design documents (drawings, specifications, etc.), prior to

issuance for use, and for approval and incorporation of changes in a formal and orderly manner. The system shall control obsolete documents to prevent inadvertent use.

5.10 Calibration Of Test And Measuring Equipment

Inspections and tests shall be performed using properly calibrated measuring and test equipment. Subcontractor shall have in its possession the necessary equipment to perform the required inspections and tests. Calibration standards shall be traceable to the National Institute for Standards and Technology (NIST) or equivalent. Subcontractor shall impose these calibration requirements on subtier suppliers.

5.11 Release For Shipment Form

Subcontractor shall have a signed "Product Quality Certification and Shipping Release" Form to be provided by PPPL's Quality Assurance Representative prior to acceptance of procured items or services for full or partial shipment. PPPL reserves the right to refuse to accept shipments unless accompanied by a signed "Shipping Release" Form .

5.12 Process History

Subcontractor shall provide, at or prior to delivery, PPPL with two (2) copies of the Process History, a compilation of documents, detailing the objective evidence of the acceptability of the work performed. The Process History shall  include as a minimum, but not be limited to, the following:

5.12.1 Certificate Of Compliance (CofC)

Subcontractor's CofC, stating that the work performed conforms in every respect to the physical configuration and functional inspection/test requirements. The CofC shall be signed by Subcontractor's Quality Assurance (QA) Manager.

5.12.2 Material Certifications

The Subcontractor shall submit copies of inspection reports, test data, and/or certifications from vendors, showing relevant chemical, mechanical and electrical properties of materials used, where applicable, as well as documents showing adherence to in-process requirements. Material certifications from sub-tier suppliers shall also be submitted.

5.12.3 Inspection/Test Documents

Copies of filled in and completed process planning and control documents (travelers, etc.) which verify controlled execution of the required work. (Records shall be available for review but may not be required for delivery.)

5.12.4 Inspection Reports

Copies of the original reports of all required inspections and examinations, properly validated by authorized personnel.

5.12.5 Test Reports

Copies of the original test data sheets or reports of all required tests, both in-process and acceptance, properly validated by authorized personnel.

5.13 PPPL RECEIVING/ INSPECTION

PPPL will perform Receiving Inspection on items or services supplied by Subcontractor, using either a sampling plan or 100% inspection. Discrepant items or services will be rejected and returned to Subcontractor or reworked by PPPL.  Costs caused by rejects will be charged to Subcontractor.

6.0 DOCUMENTATION REQUIREMENTS

6.1 Proposal Technical Documentation

Subcontractor shall submit as part of his proposal documentation in preliminary or outline form, the QA Plan (refer to section 5.4), the Inspection/Test Plan (refer to section 5.5), and procedures for tests on extruded conductors (refer to section 5.6).

6.2 Documentation After Contract Award and Prior to Fabrication

Subcontractor shall submit final versions of the QA Plan (refer to section 5.4), the Manufacturing/Inspection/Test Plan (refer to section 5.5), and procedures for tests on extruded conductors (refer to section 5.6) for PPPL review and approval in accordance with the schedules given in the referenced sections.

6.3 Documentation Prior to Shipment

Subcontractor shall submit documents identified in section 5.12, Process History.

7.0 HANDLING, SHIPPING AND STORAGE

a. The extruded conductors shall be loosely wound on spools for shipping.  The spools shall have an inner diameter of not less than three feet.  The OH copper shall be spooled with the crown side towards the outside diameter of the spool.

b. The spools shall protect the materials from shock and weather conditions, including precipitation and temperatures below freezing.  Seller’s name, shipper, purchase order number, contents and gross weight shall be marked on the shipping container.  Seller is responsible shipment and for the safe arrival of the OH and PF1 conductors at PPPL in Princeton, New Jersey, USA.

c. The materials shall be separated by size, and prepared for shipment is such a manner as to ensure acceptance by common carrier for transportation at the lowest applicable rate and to afford protection from normal hazards of transportation.

APPENDIX

List of Drawings

| DRAWING NO. | REV NO. | TITLE |
| --- | --- | --- |

| 13.A0010.0 | 0 | OH COIL CONDUCTOR DETAIL |
| --- | --- | --- |

| 13.A0011.0 | 0 | PF1A & PF1B CONDUCTOR DETAIL |
| --- | --- | --- |