National Spherical Torus Experiment

NSTX

SPECIFICATION

FOR

TF COIL CENTER STACK BUNDLE

NSTX-SPEC-13-039

Revision 0

DATED: April 12, 1997

PREPARED BY:___________________________________

J.H. Chrzanowski

REVIEWED BY:___________________________________

J.M. Spitzer

NSTX Tokamak Systems WBS Manager

REVIEWED BY:___________________________________

Charles Neumeyer

NSTX  Engineering Manager

APPROVED BY:___________________________________

P.J. Heitzenroeder

Deputy NSTX Project Manager

PRINCETON UNIVERSITY

PLASMA PHYSICS LABORATORY

(PPPL)

P.O. BOX 451

PRINCETON, N.J. 08543

| Revision | Date | TRB | Description of Change |
| --- | --- | --- | --- |

1.0 	SCOPE	5

2.0 	APPLICABLE DOCUMENTS	5

2.1 	DRAWINGS	5

2.2 	STANDARDS AND CODES	5

2.3	GENERAL STATEMENT	6

3.0 	REQUIREMENTS	6

3.1 	EQUIPMENT DEFINITION	6

3.1.1 	General Design Features	6

3.1.2 	Materials	6

3.1.2.1 Copper Conductor	6

3.1.2.2 Insulation System	7

3.1.2.3 Degreasing/Cleaning Solvent	8

3.1.2.4 Copper Primer	8

3.1.2.5 Grit Blasting Materials	8

3.1.2.6 TF Coil Core	8

3.1.2.7 Conductor Coolant Tube	9

3.1.2.8 Soft Solder	 9

3.1.2.9    End Caps	9

3.1.2.10  Press Mold Release Agent	9

3.1.2.11  Silicone Adhesive Sealer	9

3.2 	COIL  FABRICATION	9

3.2.1 	Copper Conductor Delivery	9

3.2.2 	Conductor Cleaning	9

3.2.3 	Material Protection	10

3.2.4 	Conductor Inspection	10

3.2.5 	Coolant Tube Installation	10

3.2.6 	Flow and Hydrostatic Tests	10

3.2.7 	Conductor Grit Blasting	10

3.2.8 	Cleaning After Grit Blasting	11

3.2.9 	Primer Application	11

3.2.10 Turn Insulation	11

3.2.11 Lead Area Turn Insulation	11

3.2.12 Assembly of TF Coil Conductors	11

3.2.13 Quadrant Tests-Pre-Cure	12

3.2.14 Quadrant Cure                                                                                         12

3.2.15	Quadrant Pre-Acceptance Tests	 12

3.2.16 Assembly of TF Centerstack Quadrants	12

3.2.17	Coil Bundle Press-Molding	13

3.2.18 Ground Insulation	13

3.2.19 Machining of Ground Insulation	14

3.2.20 	Post-Machining	14

3.2.21 	Evaluation of Finished Surfaces	14

3.2.22  End Cap Installation	14

4.0 	TEST REQUIREMENTS	14

4.1	 RECEIVING INSPECTION-TF CONDUCTOR	14

4.1.1	Dimensional Measurements/Inspections	14

4.1.2 	Flow and Pressure Tests:	15

4.2 	IN-PROCESS TESTING	15

4.2.1 	Tests After Quadrant Assembly and Prior to Oven Cure	15

4.2.2 	Tests After Quadrant Cure	15

4.3 	FINAL ACCEPTANCE TESTS	15

4.3.1	Inspection	15

4.3.2	Flow/Pressure Tests	16

4.3.3	Final Electrical Tests	15

5.0 	QUALITY ASSURANCE REQUIREMENTS	16

5.1 	INSPECTION/ SURVEILLANCE/AUDIT BY PRINCETON	16

5.2 	SUBCONTRACTOR’S RESPONSIBILITY FOR CONFORMANCE	17

5.3 	QUALITY ASSURANCE PLAN	17

5.4 	MANUFACTURING, INSPECTION AND TEST PLAN	17

5.5 	INSPECTION AND TEST PROCEDURES	17

5.6 	DOCUMENT TRACEABILITY AND RECORDS	17

5.7 	EQUIPMENT/MATERIAL IDENTIFICATION AND STATUS	17

5.8 	DOCUMENT REVIEW, APPROVAL AND CONTROL	18

5.9 	CALIBRATION OF TEST AND MEASURING EQUIPMENT	18

5.10 	RELEASE FOR SHIPMENT FORM	18

5.11 	PROCESS HISTORY	18

5.11.1 Certificate Of Compliance (C of C)	18

5.11.2 Material Certifications	18

5.11.3 Inspection/Test Documents	19

5.11.4 Inspection Reports	19

5.11.5 Test Reports	19

5.12 	PPPL RECEIVING/INSPECTION	19

6.0 	DOCUMENTATION REQUIREMENTS	19

6.1 	PROPOSAL TECHNICAL DOCUMENTATION	19

6.2 	DOCUMENTATION AFTER CONTRACT AWARD AND PRIOR

TO   FABRICATION	19

6.3 	DOCUMENTATION PRIOR TO SHIPMENT	20

7.0 	SHIPPING STORAGE AND HANDLING	20

8.0 	DELIVERABLES	20

APPENDIX I	TF Center Stack Bundle drawings	21

APPENDIX II	Coil Bundle/ Insulation Data	22

1.0 	SCOPE

a. This specification defines the manufacturing requirements for the National Spherical Torus Experiment (NSTX) Toroidal Field (TF) Center Stack Bundle. The Center Stack Bundle contains the inner legs of the TF coil system.

b. Subcontractor shall furnish all material, labor  and facilities necessary to complete the work as defined in the contract documents subject to the qualifications, conditions, and exceptions noted herein.

2.0 	APPLICABLE DOCUMENTS

2.1 	DRAWINGS

a. 	Drawings identified in Appendix I describe the equipment to be provided under this specification.

b. 	Dimensions in drawings and specifications refer to conditions at room temperature (20° C/ 68° F).

2.2 	STANDARDS AND CODES

a. 	Materials and manufacturing/test methods used in fabrication of the equipment covered by this specification shall comply with the latest revision, in effect at date of purchase order, of the following currently approved applicable regulations, safety codes, specifications and standards, including applicable technical definitions as acknowledged and accepted in industry.

ASTM American Society for Testing and Materials

ASTM B32-Sn95

CDA Copper Development Association

CDA Standards Handbook, Part 2 (Wrought Products)  Alloy Data,  CDA Alloy No. 10700

Conductor

Per PPPL specification NSTX-SPEC-13-036  “TF Inner Bundle Copper Conductor”.

IEEE- Institute of Electrical and Electronic Engineers

IEEE #4, Techniques for Dielectric Tests

NEMA-National Electrical Manufacturers Association

Grades and specifications for materials developed for the electric and electronics industries.

b. 	The above Standards and Codes set forth the minimum requirements.  They may be exceeded by Subcontractor with written permission from PPPL, if in Subcontractor’s judgment, superior or more economical designs or materials are available for successful and continuous operations, as required by the specification.

2.3	GENERAL STATEMENT

Subcontractor agrees, represents and warrants that all services, designs, equipment and material sold or otherwise provided to PPPL by Subcontractor comply with applicable, Federal, State and Local laws, regulations and codes, and all applicable specifications and standards including those specified above, in each case as in effect at the date or order placement. Subcontractor shall provide PPPL with a Certificate of Compliance identifying the codes, standards and regulations complied with, and any exceptions taken,  in the design and fabrication of deliverable items.

3.0 REQUIREMENTS

3.1 EQUIPMENT DEFINITION

3.1.1 	General Design Features

a. 	Dimensional characteristics of the coils are given in the drawings identified in Appendix I.

b. 	Coil bundle insulation builds are given in Appendix II.

c. Tolerances are indicated on the drawings identified in Appendix I. Strict adherence to these dimensions is critical to the assembly and performance of the subject equipment.

3.1.2 	Materials

3.1.2.1 	Copper Conductor

a. 	The conductor will be CDA alloy 10700, silver bearing copper, (25 troy ounces per ton 0.085% min.) with Yield Strength of 30-36 ksi (0.5% elongation) and Ultimate Tensile Strength 38 ksi minimum (15% elongation).

b. 	The copper conductor will be provided by PPPL.  All generated scrap and excess material furnished by PPPL shall remain the property of PPPL. A material inventory, defining quality, condition and quantity of excess material shall be maintained and submitted at the conclusion of the job. PPPL shall instruct Subcontractor as to the disposition of excess materials at PPPL’s expense.

c. 	The conductors will be supplied by PPPL to the Subcontractor with the electrical end connections and coolant tube grooves already machined in each conductor, and with  inserts ("Keenserts") already installed in the bolt holes.

3.1.2.2 	Insulation System

a. The turn insulation shall consist of "CTD-112P"  pre-impregnated (B-stage) epoxy-glass tape applied in half-lapped layers.

b. 	All of the CTD-112P tape, sheet and roving shall be provided by PPPL. All remaining insulating materials required to manufacture the TF bundle shall be provided by the Subcontractor.  All excess material furnished by PPPL shall remain the property of PPPL. A material inventory, defining quality, condition and quantity of excess material shall be maintained and submitted at the conclusion of the job.  PPPL shall instruct Subcontractor as to the disposition of excess materials at PPPL’s expense.

c.	The boundary layer between the inner and outer conductors shall consist of a layer of CTD-112 pre-impregnated epoxy-glass sheet.  An additional layer of Kapton polyimide film in sheet form without adhesive backing shall be installed between the inner and outer conductors in the vicinity of the outer conductor electrical joints.

d. 	The ground insulation shall be “Scotchply” Type No.1003 pre-impregnated (B-stage) epoxy-glass tape applied in half-lapped layers to the outside diameter of the TF bundle. The final radial build after final cure and machining shall be in accordance with the drawings identified in Appendix I.

e. The barrier between quadrants shall consist of pre-impregnated epoxy-glass sheets (provided by PPPL) with the same resin as the CTD-112P tape. This insulation shall be applied in sheet form with no splices.

f. 	Any voids between turns or near lead areas will be filled with pre-impregnated glass rope (provided by PPPL) with the same resin as the CTD-112P tape.

g. 	The dielectric shields in the joint areas shall be Kapton polyimide film in sheet form without adhesive backing.

h. 	Details concerning the insulating materials are as follows:

CTD-112P Pre-impregnated Tape and Sheet

Resin Type:	TGDM epoxy, aromatic amine cure agent

Glass tape:  S-2 ( satin weave) std. silane finish

Temperature Class:	180° C

Nominal Thk.: 	0.006 in. (0.152 mm.) tape

0.022 in. (0.508 mm) sheet

Nominal Width:  	1.0 in. tape, or  sheet form

Braided Glass Rope  (Roving)

Glass:  S-2 glass

Resin Type: 	TGDM epoxy, aromatic amine cure agent

Temperature Class:	180° C

Nominal Diameter:	0.125, 0.25 and 0.375 inch

Kapton Sheet- “Dupont” product

Type H polyimide film

Nominal Thickness:  0.004 in. (0.102 mm)

Nominal width:  Sheet form

Temperature Class:	180° C

3M-Scotchply #1003- Groundwall

Epoxy-glass pre-preg insulation in tape form

Glass Tape:  Type “K” filament

Nominal Thickness:  .010 in. (0.254 mm)

Nominal width:  2.0 in. tape

3.1.2.3 	Degreasing/Cleaning Solvent

All conductors shall be degreased/cleaned using a solvent which has been pre-approved by PPPL.  This solvent should be able to dissolve grease, tar, wax, adhesives, oils and other soils without leaving a residue.

3.1.2.4 	Copper Primer

The primer shall be Araldite DZ-80-1, manufactured by Ciba-Geigy (UK) Limited Plastics Division.  No substitutions permitted.

3.1.2.5 	Grit Blasting Materials

Grit blasting shall be performed using aluminum oxide with a grain size of 80-120 mesh.

3.1.2.6 	TF Coil Core  (Reference Dwg. 13.E0015.0)

The center core of the TF bundle assembly shall be made of silicone rubber with a Shore “A” Durometer hardness of 60.  Recommended materials include “G.E.” silicone rubber products No. RTV 31 or RTV 60. Subcontractor shall recommend suitable material and receive PPPL approval prior to fabrication of core.

3.1.2.7 	Conductor Coolant Tube

The coolant tube which shall be soldered into the TF conductors shall be seamless Air Conditioning and Refrigeration  (ACR) copper tubing with 0.312 in. outside diameter and 0.032 in. wall thickness.  The tubing shall be procured with the outside diameter pre-tinned prior to soldering into the conductor.

3.1.2.8 	Soft Solder

The copper coolant tube shall be soft-soldered into the TF conductor using 95%/5% Tin-Antimony soft-solder with a melt range of 453-464 °F.  Subcontractor shall recommend suitable liquid flux.  Any changes from this shall require PPPL approval.

3.1.2.9	End Caps  (Reference Drawing 13.E0042.0)

The TF Bundle end caps shall be made of NEMA Grade G-10 glass reinforced epoxy, meeting all NEMA (National Electrical Manufacturers Association) “G-10” Grade specifications.

3.1.2.10	Press-Mold Release Agent

A suitable press-mold release agent shall be recommended by the subcontractor and approved by PPPL.

3.1.2.11	Silicone Adhesive Sealer

A suitable silicone adhesive sealer for securing the end caps in position shall be recommended by the subcontractor and approved by PPPL.

3.2 	COIL  FABRICATION

This section describes a recommended procedure for fabricating the subject equipment.  The Subcontractor shall submit for approval by PPPL, a Manufacturing, Inspection, and Test (MIT) plan.  No deviations from the MIT plan will be accepted without PPPL approval.

3.2.1 Copper Conductor Delivery

The copper conductors shall be delivered to the Subcontractor with the electrical contact face of each conductor end individually wrapped for protection.  The crates shall be inspected for visual damage by the Subcontractor and condition of crates documented.

3.2.2 Conductor Cleaning

Each conductor shall be wiped down with degreasing solvent to remove excess oil, lubricant and grease.

3.2.3 	Material Protection

Cleaned copper, whether bare or insulated, shall be stored and processed in an environment free from metallic dust or other contaminants.  The copper surface and insulating materials shall be protected from skin oil, etc., by requiring shop personnel to handle conductors only while wearing clean, lint free, white cotton gloves.  Insulation and in-process subassemblies shall be processed and stored in controlled clean areas.  The electrical joint faces at each end of the conductors shall be protected from damage.

3.2.4 	Conductor Inspection

The copper conductors shall be moved to an inspection table where they shall be inspected per requirements in Section 4.0 paragraph 4.1.

3.2.5 	Coolant Tube Installation

a.	The pre-tinned copper coolant tube shall be positioned and soft-soldered into the groove provided in each conductor.  The copper tube shall be continuous with no splices.  ( Reference Drawing 13.E0016.0)

b.	Caution:  Extreme care must be taken to ensure that the heating process used for soldering does not effect the hardness of the copper extrusion.  Pre and post  Rockwell hardness measurements shall be taken by subcontractor to ensure compliance. This information shall be included in the Process History.

c.	Following the soldering operation, the excess solder shall be removed from the conductor so that the cross-section of the conductor conforms to the PPPL drawings.  Care should be taken so that the coolant tube is not damaged.  The conductor must also be cleaned to remove flux residue.

3.2.6	Flow and Hydrostatic Tests:

Flow and hydrostatic tests of the soft-soldered coolant tube shall be performed per requirements in section 4.1.2 to verify integrity of the coolant tube and to provide a base line for future tests.

3.2.7 	Conductor Grit Blasting

Following the installation and testing of the coolant tubes, the conductor shall be grit blasted to remove any surface oxidation and promote insulation bonding.  This process must be performed in a controlled  manner which will expose the conductor to grit blasting at a recommended rate of 12 seconds/ inch2. It is essential that water and oil filters are located in the main air supply line to minimize the risk of introducing contaminants onto the conductors.

3.2.8	Cleaning After Grit Blasting

After grit blasting, the conductor shall be vacuum cleaned and wiped to remove all residue remaining from the grit blasting.

3.2.9	Primer Application

A layer of DZ-80-1 primer will be applied by brushing or spraying. The final method for application and curing must be approved by PPPL.  It is important that the primer be applied with a thin uniform thickness.  Primer shall be air dried before proceeding.  The final cure of the primer shall occur during the insulation cure cycle.

3.2.10 	Turn Insulation

a. 	The half-lapped layers of turn insulation shall be applied to the conductors to achieve the cured insulation thickness specified on the drawings and in appendix II.

b. 	Care shall be taken to avoid damage to the insulation in subsequent handling.  Damaged insulation shall be replaced with new insulation in accordance with a Subcontractor Prepared/ PPPL approved repair procedure which will maintain insulation continuity.

3.2.11 	Lead Area Turn Insulation

Turn insulation shall be tailored to fit neatly around water and electrical terminals.

3.2.12 Assembly of TF Coil Conductors

a. 	Insulated TF conductors shall be assembled in accordance with approved drawings to form a quadrant of the TF bundle. Joint surfaces at each end of the bundle shall be precisely located in angular position by bolting a tooling fixture (designed and supplied by Subcontractor, approved by PPPL) into the inserts ("Keenserts") provided in the bolt holes. Fixture shall be designed to provide angular alignment and to permit, or assist in, the application of  inward radial compression during cure. Maximum allowable bolt tension is TBD pounds.

b. 	All voids between turns shall be filled with B-stage roving.

c.	A layer of CTD-112 pre-impregnated epoxy-glass sheet shall be placed between the inner and outer row of insulated conductors.  In the vicinity of the outer TF electrical connection areas (2) locations an additional layer of Kapton polyimide film, in sheet form without adhesive backing, shall be positioned between the inner and outer row of insulated conductors.

d. 	Kapton dielectric shields shall be positioned between the TF conductors at the electrical connection areas. (Reference Drawing 13.E0016.0)

e.	Two (2) half-lapped layers of 2 mil non-stick (Tedlar) tape shall be applied around the entire quadrant.

f. 	Two (2) half-lapped layers of shrinkable mylar tape shall be applied over the Tedlar layer.

3.2.13	Quadrant Test- Pre-Cure

Each conductor within the TF Coil quadrant shall be electrically tested against all other conductors shorted together and grounded per test requirements given in section 4.

3.2.14	Quadrant Cure

a. 	Internal surfaces of a press mold (design and supplied by Subcontractor, approved by PPPL) shall be coated with pre-approved mold release agent.  The TF quadrant shall be installed into the press mold. The press mold shall be designed to provide sufficient compression of the B-stage insulating materials to insure that the resin flows into all voids and that the dimensions of the finished assembly are within the specified tolerances.

b. 	The quadrant bundle and press mold shall be heated in an oven, and cured at 170° C for a period of (2) two hours.  During this time the press mold shall apply sufficient compression (10% of nominal B-stage insulation thickness) to the quadrant to allow the conductors to form a monolithic, void free structure with dimensions within the specified tolerances.

c. 	The subcontractor shall monitor and record cure temperature and time during the entire cure process.  This information shall become part of the Process History per section 5.11.

d. 	Following the insulation cure cycle, the quadrant shall be removed from the press mold. The layers of Tedlar and shrinkable mylar shall be removed and the quadrant bundle inspected.

3.2.15 Quadrant Pre-Acceptance Tests

Each conductor within the TF Coil quadrant shall be electrically tested against all other conductors shorted together and grounded per test requirements given in section 4.

3.2.16 Assembly of TF Centerstack Quadrants

a. The four quadrants shall be assembled together to form the complete bundle assembly. Joint surfaces at each end of the bundle shall be precisely located in angular and axial position by bolting a tooling fixture (designed and supplied by Subcontractor, approved by PPPL) into the inserts ("Keenserts") provided in the bolt holes. Fixture shall be designed to provide angular alignment and axial location and to permit, or assist in, the application of inward radial compression during cure. Maximum allowable bolt tension is TBD pounds.

b.  Two (2) layers of CTD-112P Prepreg insulation shall be applied between each quadrant.  This barrier shall be applied in sheet form to provide a continuous bond surface.

c. 	The silicone rubber core in the center of the TF bundle shall be included during the assembly operation. Care shall be taken to ensure that the surfaces of the silicone rubber core have been cleaned prior to installation.

d. 	All voids between turns shall be filled with prepreg roving.

3.2.17 Coil Bundle Press-Molding

a.  Two (2) half-lapped layers of 2 mil non-stick (Tedlar) tape shall be applied around the entire TF bundle.

b.  Two (2) half-lapped layers of shrinkable mylar tape shall be applied over the Tedlar layer.

c. 	The internal surfaces of the press mold shall be coated with pre-approved mold release agent.

d.  The TF coil bundle shall be transported to the oven area and placed in a press mold.  The press-mold shall be designed to provide sufficient compression of the B-stage insulating materials to insure that the resin flows into all voids and that the dimensions of the finished assembly are within the specified tolerances.

e. 	The coil bundle and mold shall be heated and cured to the following times and temperatures.

2 hours @ 177°C

7 hours @ 200°C

During this time the press mold shall apply sufficient compression (10% of nominal uncured B-stage insulation thickness) to the TF bundle to allow the quadrants to form a monolithic, void free structure with dimensions within the specified tolerances.

f.  Following the insulation cure cycle, the TF coil bundle shall be removed from the press-mold. The layers of Tedlar and shrinkable mylar shall be removed, and the coil bundle shall be inspected.

3.2.18 Ground Insulation

a. 	The ground insulation shall be applied to the outside diameter of the assembled TF bundle using half-lapped layers of pre-preg Scotchply #1003 insulation.

b. 	All layers of ground insulation shall be applied in the same direction.

c. 	The ground insulation build up shall result in an oversized diameter allowing additional insulation thickness for machining. Subcontractor shall  determine the required buildup with PPPL approval.

d.	The ground insulation shall be tailored to fit neatly around the conductor end electrical flags.

e. 	The “Scotchply” ground insulation shall be cured to mutually agreed upon specifications.

3.2.19 Machining of Ground Insulation

a. 	After the “Scotchply” has cured, the TF coil ground insulation shall be machined to achieve the final dimensions as specified in the drawings.

b.	The method for machining the ground insulation of the TF Bundle shall be proposed by Subcontractor and approved by PPPL. Care must be taken not to machine below the specified dimensions in the drawings.

3.2.20 Post-Machining

Subcontractor shall evaluate the machined coil bundle surfaces to verify freedom from defects such as cracks, dry spots, voids, etc.  The coil bundle surfaces shall not be patched or mechanically processed without written approval of PPPL. There shall be no voids or delaminations.  Surface cracks shall be reviewed with PPPL for disposition.

3.2.21 Evaluation of Finished Surfaces

The cured coils shall be checked for dimensional conformance with the drawings.

3.2.22  End Cap Installation

Subcontractor shall install G-10 End Caps on each end of the TF Bundle.  Silicone adhesive sealer  (RTV) shall be used to secure the end caps in position.

4.0 TEST REQUIREMENTS

Mechanical and electrical inspections and tests shall be performed on each quadrant.  Test points, test methods, acceptance criteria, and PPPL witness points shall be described in the Manufacturing Inspection Test (MIT) Plan.

4.1 RECEIVING INSPECTION-TF CONDUCTOR

4.1.1 Dimensional Measurements/Inspections

a. 	Conductors shall be checked to verify that length and cross sectional dimensions are within the required tolerance on the approved PPPL drawings.  They will also be inspected for twist, warp and camber.

b. 	The dc resistance and temperature of each conductor shall be measured and recorded.

4.1.2 Flow and Pressure Tests:

Following the installation of the coolant tubes into the conductors the following flow and pressure test shall be performed.

a. 	The soft-soldered edge coolant tube in each TF conductor must be tested for flow, and hydrostatic tests to verify the integrity of the coolant tube and to provide a base line for future tests.  These tests shall be performed using potable water.

b.	Operational flow rates and pressure drops are as follows:

16 gpm          35 ± 5 psi pressure drop

c. 	The hydrostatic pressure shall be 600 psi for 30 minutes with no leaks.  The pressure vs. time data shall be recorded.

4.2 IN-PROCESS TESTING

4.2.1 Tests After Quadrant Assembly and Prior to Oven Cure

Once the TF conductors have been assembled into a TF Quadrant bundle, the insulation between each inner leg within the quadrant shall be verified by applying a 500 Volt Megger for a minimum of 2 minutes between each individual turn and the remainder of the turns, which shall be shorted and grounded.  Insulation resistance shall be greater than 1000 MΩ.

4.2.2 Tests After Quadrant Cure

Once the conductors for a TF coil center stack quadrant have been cured and prior to being assembled into the full bundle, the insulation between each inner leg within the quadrant shall be verified by applying a 3 kV Megger between each individual turn and the remainder of the turns, which shall be shorted and grounded.   Insulation resistance shall be greater than 1000 MΩ.

4.3 FINAL ACCEPTANCE TESTS

These tests and inspections shall be performed once the TF Center Stack Bundle is in a deliverable configuration.

4.3.1	Inspection

A careful visual inspection and dimensional check shall be made according to applicable drawings. All dimensions shall be in conformance with the drawings.

4.3.2	Flow/Pressure Tests

A final flow and hydrostatic pressure test of the soft-soldered edge coolant conductor tubes shall be performed to verify that no tube damage has been done to the soft-soldered tube as a result of final processing of the TF Center Stack Bundle.  These tests shall be performed using potable water. Operational flow rates and pressure drops shall be within 10% of the data collected in section 4.1.2.

4.3.3	Final Electrical Tests

a. 	Coils shall be temporarily wrapped with conducting material (e.g. Al foil) to provide a ground plane.

b.  The insulation between each inner leg within the quadrant, and to ground, shall be verified by applying a 3 kV Megger between each individual turn and the remainder of the turns, which shall be shorted and grounded.  Insulation resistance shall be greater than 1000 MΩ.

c. 	The insulation between the coil bundle and ground shall be verified by applying a 3 kV DC Hipot between all turns, shorted together, and ground. Voltage shall be ramped up in 10 seconds, held for 60 seconds, and ramped down in 10 seconds.  Leakage current shall be recorded during ramping up and down, and once every 10 seconds during the 60 second interval.  Leakage current shall not exceed 10 µ Amps.

5.0 	QUALITY ASSURANCE REQUIREMENTS

5.1 	INSPECTION/ SURVEILLANCE/AUDIT BY PRINCETON

Authorized representatives of PPPL and the U. S. Government shall have the right at all reasonable times to visit the Subcontractor's premises and those of Subcontractor's suppliers during the performance of the procurement for the purposes of inspection, surveillance, audit and/or obtaining any required information as may be necessary to assure that items or services are being furnished in accordance with specified requirements. Such visits shall be coordinated with the Subcontractor's personnel to minimize interference with the normal operations of said premises. The Subcontractor shall make available records and documentation necessary for this function and shall provide all reasonable facilities and assistance for the safety and convenience of PPPL and/or U. S. Government representatives in the performance of their duties.   PPPL and the U. S. Government recognize the Subcontractor's right to withhold information concerning proprietary processes. The Subcontractor agrees to insert the paragraph above in each lower tier procurement issued hereunder.

5.2 	SUBCONTRACTOR’S RESPONSIBILITY FOR CONFORMANCE

Neither PPPL's review and/or approval of Subcontractor's documents nor PPPL's inspection of Subcontractor's items or services shall relieve the Subcontractor of responsibility for full compliance with requirements of the purchase order/contract.

5.3 	QUALITY ASSURANCE PLAN

Subcontractor shall submit as soon as practical after the subcontract/purchase order award, two (2) copies of its Quality Assurance Plan, describing the specific quality assurance and quality control procedures and practices to meet the requirements of this particular subcontract/purchase order, for PPPL review and approval.

5.4 	MANUFACTURING, INSPECTION AND TEST PLAN (MIT)

Subcontractor shall prepare and submit for PPPL review and approval a Manufacturing/Inspection/Test Plan which identifies parts, sub-assemblies, etc.; shows their integrated flow into end items; and identifies critical manufacturing operations as well as inspections and tests. Preparing the Plan may include developing a flow chart and generating Process Sheets/Shop Travelers, etc. PPPL may designate selected manufacturing, inspection and/or test operations as mandatory “witness” points based on the MIT plan. Subcontractor shall provide PPPL with five (5) working days notice in advance of such witness points.

5.5 	INSPECTION AND TEST PROCEDURES

Inspections and tests shall be performed in accordance with written procedures referencing criteria for acceptance or rejection.  Adequate records shall be maintained and available for PPPL's review.

5.6 	DOCUMENT TRACEABILITY AND RECORDS

The Subcontractor shall maintain a system of documentation whereby objective evidence of required operations, inspections, examinations, and tests is systematically compiled, indexed and stored.  Such objective evidence may include "travelers"; and material test, certification, inspection, examination, test and discrepancy reports; which shall be complete, legible, and validated by responsible personnel and shall be traceable to subject items.

5.7 	EQUIPMENT/MATERIAL IDENTIFICATION AND STATUS

Material and equipment identification shall be maintained throughout the program and be traceable to the records. Status of acceptability shall be readily discernible through the Subcontractor's use of tags, stamps, serial numbers or other positive means.

5.8 	DOCUMENT REVIEW, APPROVAL AND CONTROL

The Subcontractor shall provide a system for distribution and control of approved documents and changes thereto. The system shall use procedures which provide for review and approval of design documents (drawings, specifications, etc.), prior to issuance for use, and for approval and incorporation of changes in a formal and orderly manner. The system shall control obsolete documents to prevent inadvertent use.

5.9 	CALIBRATION OF TEST AND MEASURING EQUIPMENT

Inspections and tests shall be performed using properly calibrated measuring and test equipment. Subcontractor shall have in its possession the necessary equipment to perform the required inspections and tests. Calibration standards shall be traceable to the National Institute for Standards and Technology (NIST) or equivalent. Subcontractor shall impose these calibration requirements on subtier suppliers.

5.10 	RELEASE FOR SHIPMENT FORM

Subcontractor shall have a signed "Product Quality Certification and Shipping Release" Form to be provided by PPPL's Quality Assurance Representative prior to PPPL acceptance of procured items or services for full or partial shipment. PPPL reserves the right to refuse to accept shipments unless accompanied by a signed "Shipping Release" Form .

5.11 	PROCESS HISTORY

Subcontractor shall provide to PPPL a Process History which includes a compilation of documents, detailing the objective evidence of the acceptability of the work performed. The Process History shall  include as a minimum, but not be limited to, the following:

5.11.1 Certificate Of Compliance (C of C)

Subcontractor's C of C, stating that the work performed conforms in every respect to the physical configuration and functional inspection/test requirements. The C of C shall be signed by Subcontractor's Quality Assurance (QA) Manager.

5.11.2 Material Certifications

The Subcontractor shall submit copies of inspection reports, test data, and/or certifications from vendors, showing relevant chemical, mechanical and electrical properties of materials used, where applicable, as well as documents showing adherence to in-process requirements. Material certifications from sub-tier suppliers shall also be submitted.

5.11.3 Inspection/Test Documents

Copies of filled in and completed process planning and control documents (travelers, etc.) which verify controlled execution of the required work. (Records shall be available for review but may not be required for delivery.)

5.11.4 Inspection Reports

Copies of the original reports of all required inspections and examinations, properly validated by authorized personnel.

5.11.5 Test Reports

Copies of the original test data sheets or reports of all required tests, both in-process and acceptance, properly validated by authorized personnel.

5.12 PPPL RECEIVING/INSPECTION

PPPL will perform Receiving Inspection on items or services supplied by Subcontractor, using either a sampling plan or 100% inspection. Discrepant items or services will be rejected and returned to Subcontractor or reworked by PPPL.  Costs caused by rejects will be charged to Subcontractor.

6.0 DOCUMENTATION REQUIREMENTS

6.1 	PROPOSAL TECHNICAL DOCUMENTATION

a. 	Subcontractor shall submit as part of his proposal documentation in preliminary or outline form, the QA Plan (refer to section 5.3), the Manufacturing/Inspection/Test Plan (refer to section 5.4), and procedures for tests (refer to section 5.5).

b. Subcontractor shall submit as part of the proposal a preliminary description of the press mold and conductor alignment fixtures (refer to sections 3.2.12, 3.2.14, 3.2.16 and 3.2.17).

6.2 	DOCUMENTATION AFTER CONTRACT AWARD AND PRIOR TO   	FABRICATION

a. 	Subcontractor shall submit (2 copies) final versions of the QA Plan (refer to section 5.3), the Manufacturing/Inspection/Test Plan (refer to section 5.4), and procedures for tests (refer to section 5.5) for PPPL review and approval within 30 days of contract award.

b. 	Subcontractor shall submit (2 copies) a final description of the press mold and conductor alignment fixtures (refer to sections 3.2.12, 3.2.14, 3.2.16 and 3.2.17)  for PPPL review and approval within 30 days of contract award.

c. 	Subcontractor shall submit (2 copies) of final fabrication drawings for PPPL review and approval within 30 days of contract award.

6.3 	DOCUMENTATION PRIOR TO SHIPMENT

a. 	Subcontractor shall submit (2 copies) all documents identified in section 5.11, Process History.

b. Subcontractor shall submit an inventory of excess materials provided by PPPL.

7.0 	SHIPPING STORAGE AND HANDLING

a. 	The conductor coolant tubes shall be drained of all water and sealed for storage and subsequent shipment.

b. 	The center stack bundle shall be crated for shipment.  The crate shall be built for moving on rollers, handling with slings from overhead cranes and forklifts.

c. The crate shall protect the center stack bundle from shock and weather conditions, including precipitation and protection against freezing.  Subcontractor’s name, shipper, purchase order number, contents and gross weight shall be marked on the shipping container.  Subcontractor is responsible arranging shipment, and for the safe arrival of the TF Center Stack Bundle at PPPL in Princeton , New Jersey, USA.

d. 	The TF Bundle shall be prepared for shipment is such a manner as to ensure acceptance by common carrier for transportation at the lowest applicable rate and to afford protection from normal hazards of transportation.

8.0 	DELIVERABLES

The Subcontractor is responsible for delivering to PPPL the following:

a. 	All documentation listed in section 6.0.

b. 	One (1) completed TF Coil Center Stack Bundle which has successfully passed all acceptance tests and criteria.

c.	Balance of materials supplied by PPPL or which were procured by Subcontractor solely for this contract.

d. 	Fixtures or tooling fabricated solely for the fabrication of the TF Center Stack Bundle.

APPENDIX I

TF Center Stack Bundle drawings

| Description | PPPL Drawing Number |
| --- | --- |

| Inner TF Conductor | NSTX 13.E0025.0 |
| --- | --- |

| Outer TF Conductor | NSTX 13.E0026.0 |
| --- | --- |

| Conductor/Insulation Arrangement | NSTX 13.E0100.D |
| --- | --- |

| Inner Coil Quadrant Assembly Conductor Insulation Arrangement Protective End Cap Details | NSTX 13.E0016.0 NSTX 13.E0015.0 NSTX-13.E0042.0 |
| --- | --- |

APPENDIX II

Coil Bundle/ Insulation Data

|  | Dimension (in.) | Radius (in.) | Dimension (cm.) | Radius (cm.) |
| --- | --- | --- | --- | --- |

| TF Quadrant Radial Build |  |  |  |  |
| --- | --- | --- | --- | --- |

| TF Centerbore | 0.250 | 0.250 | 0.635 | 0.635 |
| --- | --- | --- | --- | --- |

| 1st. layer turn Insulation (IR cu) | 0.032 | 0.282 | 0.081 | 0.716 |
| --- | --- | --- | --- | --- |

| 1st. layer copper conductor (OR) | 1.936 | 2.218 | 5.634 | 5.634 |
| --- | --- | --- | --- | --- |

| 1st. layer turn insulation | 0.032 | 2.250 | 0.081 | 5.715 |
| --- | --- | --- | --- | --- |

| TF Layer Insulation | 0.020 | 2.270 | 0.051 | 5.766 |
| --- | --- | --- | --- | --- |

| 2nd. layer turn insul. (copper) | 0.032 | 2.282 | 0.081 | 5.847 |
| --- | --- | --- | --- | --- |

| 2nd. layer (conductor face) | 1.546 | 3.828 | 3.268 | 9.774 |
| --- | --- | --- | --- | --- |

| 2nd. layer turn insulation | 0.032 | 3.860 | 0.081 | 9.855 |
| --- | --- | --- | --- | --- |

| TF Bundle Build |  |  |  |  |
| --- | --- | --- | --- | --- |

| At (0°, 90°, 180° & 270°) |  |  |  |  |
| --- | --- | --- | --- | --- |

| Allowance for Segment insulation | 0.020 | 3.900 | 0.051 | 9.906 |
| --- | --- | --- | --- | --- |

| TF Groundwall | 0.062 | 3.962 | 0.157 | 10.064 |
| --- | --- | --- | --- | --- |

| At (45°, 135°, 225° & 315°) |  |  |  |  |
| --- | --- | --- | --- | --- |

| Allowance for Segment insulation | 0.028 | 3.908 | 0.072 | 9.927 |
| --- | --- | --- | --- | --- |

| TF Groundwall | 0.054 | 3.962 | 0.137 | 10.064 |
| --- | --- | --- | --- | --- |

Note:  Turn to Turn Insulation builds are based upon 10% compression of nominal B-stage insulation thickness.