October 18, 1996

To: BJ Lee

From: Wayne Reiersen

Subject: SUPERCODE Benchmarking against TPX

Per our agreement, I am providing you with data from detailed engineering calculations of the TPX baseline.  I believe you have the data necessary to benchmark the code against the detailed physics calculations already.

Pertinent data for the design of the TF coils are provided in Table 1.  There are a few important differences between the SuperCode output which you provided and the reference TPX values, notably:

•	The cable area in SuperCode is 20% larger.

•	The number of strands in the conductor is 30% larger.

•	The maximum primary membrane stress in the case is twice as high.

•	The helium temperature at the location of peak field should be 6K, not the inlet temperature of 5K.  The highly erroneous temperature margin and fraction of critical are at least in part due to the incorrect temperature.

Table 1 - TPX TF Parameters

| TF Parameter | Units | SuperCode | TPX |
| --- | --- | --- | --- |

| TF edge ripple | % | 0.238 | 0.28 |
| --- | --- | --- | --- |

| TF peak field with ripple | T | 7.46 | 8.4 |
| --- | --- | --- | --- |

| Number of coils |  | 16 | 16 |
| --- | --- | --- | --- |

| Stored energy | GJ | 1.11 | 1.08 |
| --- | --- | --- | --- |

| Straight section height | m | 1.68 | 1.17 |
| --- | --- | --- | --- |

| Vertical clear bore | m | 4.80 | 4.35 |
| --- | --- | --- | --- |

| Horizontal clear bore | m | 2.56 | 2.56 |
| --- | --- | --- | --- |

| Radius of peak field | m | 1.258 | 1.23 |
| --- | --- | --- | --- |

| Cable area (cond + void) | mm2 | 465 | 392 |
| --- | --- | --- | --- |

| Conduit thickness | mm | 2.41 | 2.41 |
| --- | --- | --- | --- |

| Conduit area/turn | mm2 | 234 | 192 |
| --- | --- | --- | --- |

| Cable aspect ratio (radial/toroidal) |  | 1 | 1.3 |
| --- | --- | --- | --- |

| Strand diameter | mm | ??? | 0.78 |
| --- | --- | --- | --- |

| Strands per conductor turn |  | 629.9 | 486 |
| --- | --- | --- | --- |

| Conductor fraction |  | .382 | .37 |
| --- | --- | --- | --- |

| Copper fraction (of conductor) |  | .778 | .714 |
| --- | --- | --- | --- |

| Structure fraction |  | .298 | .29 |
| --- | --- | --- | --- |

| Insulation fraction |  | .111 | .11 |
| --- | --- | --- | --- |

| Helium fraction |  | .209 | .21 |
| --- | --- | --- | --- |

| Winding radial thickness | m | .2017 | .214 |
| --- | --- | --- | --- |

| Winding toroidal thickness | m | .3263 | .291 |
| --- | --- | --- | --- |

| Current per turn | kA | 33.63 | 33.48 |
| --- | --- | --- | --- |

| Turns per coil |  | 83.63 | 84 |
| --- | --- | --- | --- |

| Primary membrane stress/Sm | MPa | 725/550 | 322/543 |
| --- | --- | --- | --- |

| Helium inlet temperature | K | ? | 5 |
| --- | --- | --- | --- |

| Helium temperature @ peak field | K | 5 | 6.0 |
| --- | --- | --- | --- |

| Helium fraction inside cable |  | .353 | .353 |
| --- | --- | --- | --- |

| Conductor strain | % | ? | 0.36 |
| --- | --- | --- | --- |

| Conductor copper fraction |  | .67 | .71 |
| --- | --- | --- | --- |

| Critical current | kA | 120 | 56 |
| --- | --- | --- | --- |

| Op current/critical current |  | .28 | 0.60 |
| --- | --- | --- | --- |

| Temperature margin | K | 5.9 | 2.0 |
| --- | --- | --- | --- |

| Temperature headroom | K | ? | 3.0 |
| --- | --- | --- | --- |

| Max temp in dump | K | 150 | 151 |
| --- | --- | --- | --- |

| J limit protection | kA/cm2 | 7.6 | 14.4 |
| --- | --- | --- | --- |

| Quench detection time | s | ? | 1 |
| --- | --- | --- | --- |

| Dump time | s | 5.5 | 4 |
| --- | --- | --- | --- |

| Dump voltage | kV | 12 | 15 |
| --- | --- | --- | --- |

| I_op/I_transition |  | 0.63 | ? |
| --- | --- | --- | --- |

| Nuclear heating in winding | kW | ? | 3.95 |
| --- | --- | --- | --- |

| Nuclear heating in cold structure | kW | 4.4 | 6.7 |
| --- | --- | --- | --- |

| Eddy current heating in cold structure | kW | 2.4 | 1.4 |
| --- | --- | --- | --- |

| Indirect heat load to winding | kW | ? | 0.82 |
| --- | --- | --- | --- |

| Total heat load removed in winding | kW | ? | 4.77 |
| --- | --- | --- | --- |

PF geometric parameters are shown in Table 2.  SuperCode values are listed above the reference values.  SuperCode breaks the central solenoid into two pieces, roughly equivalent to PF1,2 and PF3,4.  Notable differences include the following:

•	The radial builds of the CS winding are different.

•	The PF1,2 equivalent is substantially taller, 1.057m versus 0.886m.

•	The aspect ratio of the ring coils are fixed at unity whereas in the reference design, the aspect ratios ranged from 2-3.3.  The has a strong impact on peak field values, if they are used.

•	The area and number of turns in PF6 were grossly low.

•	The number of turns in PF7 was also low although the areas were comparable.

| Coil | R_a | R_b | Z_a | Z_b | AR | Area(m2) | Turns |
| --- | --- | --- | --- | --- | --- | --- | --- |

| PF1/2 | 0.718 | 0.917 | 0 | 1.057 |  | 0.210 | 338 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 0.738 | 0.882 | 0.012 | 0.49 |  | 0.124 | 216 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 0.738 | 0.882 | 0.515 | 0.898 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |

| PF3/4 | 0.718 | 0.917 | 1.057 | 1.457 |  | 0.080 | 114 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 0.738 | 0.882 | 0.922 | 1.161 |  | 0.069 | 120 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 0.738 | 0.882 | 1.186 | 1.425 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |

| PF5 | 1.313 | 1.687 | 2.458 | 2.832 | 1 | 0.140 | 112 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 1.117 | 1.309 | 2.159 | 2.541 | 2.0 | 0.073 | 128 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| PF6 | 3.545 | 3.713 | 1.996 | 2.164 | 1 | 0.028 | 23 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 3.687 | 3.830 | 1.905 | 2.383 | 3.3 | 0.068 | 120 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| PF7 | 4.289 | 4.495 | 1.017 | 1.223 | 1 | 0.042 | 34 |
| --- | --- | --- | --- | --- | --- | --- | --- |

|  | 4.225 | 4.369 | 0.946 | 1.281 | 2.3 | 0.048 | 84 |
| --- | --- | --- | --- | --- | --- | --- | --- |

The performance parameters differ significantly from the TPX baseline but are certainly in the ballpark.  With SuperCode breaking the central solenoid into 2 pieces which do not cleanly map into the 4 pieces in the baseline design, it is difficult to make exact comparisons.  The difficulty is exacerbated because SuperCode apparently does not apply the same design constraints to the PF design as it does to the TF design (fraction of critical, temperature margin, etc.).  Part of the mismatch is due to the different thicknesses for the winding pack.  Overall, SuperCode predicted a volt-second capability which was 15% higher than the baseline.  This is due in part to having a substantially (30%) higher field in the PF1,2 equivalent coil at the end of flattop than the baseline design apparently would allow.  Also, the currents required in the divertor coil (PF5) are underestimated at EOF which results in the volt-seconds being overestimated.

| Coil | I_BOP (MA) | J_BOP (kA/cm2) | B_BOP (T) | I_EOF (MA) | J_EOF (kA/cm2) | B (T) |
| --- | --- | --- | --- | --- | --- | --- |

| PF1,2 | 3.78 | 1.80 |  | -6.72 | 3.20 | 6.34 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 1.100 | 1.60 | 4.483 | -2.597 | 3.77 | 4.82 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 2.363 | 4.28 | 5.957 | -1.079 | 1.96 | 3.59 |
| --- | --- | --- | --- | --- | --- | --- |

| PF3,4 | 2.84 | 3.58 | 6.04 | 0.8 | 1.0 |  |
| --- | --- | --- | --- | --- | --- | --- |

|  | 1.393 | 4.05 | 5.734 | -0.186 | 0.54 | 2.26 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 1.537 | 4.47 | 5.690 | -0.008 | 0.02 | 1.32 |
| --- | --- | --- | --- | --- | --- | --- |

| PF5 | 2.80 | 2 | 3.4 | 0.8 | 0.57 |  |
| --- | --- | --- | --- | --- | --- | --- |

|  | 2.077 | 2.85 | 3.499 | 2.465 | 3.38 | 3.36 |
| --- | --- | --- | --- | --- | --- | --- |

| PF6 | 0.105 | 0.38 |  | -0.567 | 2 | 1.37 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 0.050 | 0.07 | 0.148 | -1.086 | 1.60 | 1.55 |
| --- | --- | --- | --- | --- | --- | --- |

| PF7 | 0.076 | 0.18 |  | -0.852 | 2 | 1.47 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 0.265 | 0.06 | 0.395 | -0.914 | 1.90 | 1.40 |
| --- | --- | --- | --- | --- | --- | --- |

| V-s | 9.657 |  |  | -11.722 | Δ | -21.379 |
| --- | --- | --- | --- | --- | --- | --- |

|  | 8.974 |  |  | -9.750 | Δ | -18.72 |
| --- | --- | --- | --- | --- | --- | --- |

cc:	John Perkins

John Galambos

KSTAR files

Fatigue limits and bolt stresses were limiting, not primary membrane stresses