## Slide 1: Post FY16 initial in vessel inspections
F. Scotti, C. Skinner, S. Gifford
PPPL B318
2:00 PM Thursday Sept 29th 2016

## Slide 2: Purpose:
Comparison of before/after in-vessel photos
Initial assessment of any corrective actions.
  Any additional metrology request
Unedited photo-survey available at:
  smb://filesrv1.pppl.gov/photo-drop$/Drop Photos Here/Elle’s Folder/NSTXU ENTRY 09_16_2016
  P:\Photo Drop\Drop Photos Here\Elle's Folder\NSTXU ENTRY 09_16_2016
  Presentation and pictures from this presentation at http://nstx.pppl.gov/DragNDrop/Operations/In_vessel_inspections/Post_run_2016/

## Slide 3: Initial in-vessel inspections revealed vessel in good conditions, few minor issues
Opportunity for post-plasma inspection without lithiumization
Overall, no evident major issues
A few things to be noted:
  One chipped tile: outboard divertor Row 2, I – top
  A few leading edges in upper divertor outboard tiles
  Flaking aerodag on new port covers (Bay I, J)
  Flaking coatings on several midplane components
  Four “black tiles”
  Others misc.: arcs, lithium dust, …

## Slide 4: In-vessel fisheye view before campaign 12/05/2014

## Slide 5: In-vessel fisheye view after campaign 09/19/2016

## Slide 6: Over-style row 2 tile cracked on non-leading edge in upper outboard divertor in Bay I
Note leading edges
Stainless steel shard
Hypothesis: Heating / thermal expansion of protruding tile edge closed overlay/underlay gap and caused breakage

## Slide 7: Over-style row 2 tile cracked on non-leading edge in upper outboard divertor in Bay I

## Slide 8: Metallic chip peaking from behind cracked tile also exposed to plasma

## Slide 9: Tile edge shattered in three pieces, found in the CHI gap (between Bay G and Bay K)
Continuity of arcs/deposition on tile suggest tile did not crack during initial bakeout

## Slide 10: Metrology of broken tile planned
Romer arm measurements
Work Permit 2016277
Recommend engineering task to:
Establishment of maximum permissible tile protrusion (related to design value of overlay/underlay gap).
Fabrication of specialized tool with feeler gauges for rapid detection of tile protrusion over limit.
In-vessel survey of all tiles and adjustment of any tiles over limit.
Potential tool:
Flat plate with 4 feeler gauges
tile
tile
Contact ?

## Slide 11: Asymmetric erosion also observed at other toroidal locations in the upper divertor
Full image available in Drag&Drop

## Slide 12: No signs of misalignments in lower divertor tiles (both inner and outer)

## Slide 13
Bay I
Aerodag coating on new I, J mid port covers flaked off, accumulated at bottom of port
Bay J

## Slide 14: Aerodag coating on new I, J mid port covers flaked off, accumulated at bottom of port
Although it’s carbon, dust/particulate can be an issue
Bay J

## Slide 15
Bay J
Aerodag coating on new I, J mid port covers flaked off, accumulated at bottom of port

## Slide 16: Four darker tiles observed on CS, baked differently before the run?
Already observed during the run

## Slide 17: Arc apparent on Bay I mid deposition monitor
Needed to be disconnected during plasma ops to avoid ground fault (to be investigated)

## Slide 18: Lithium carbonate dust still around in the vessel, as observed during plasma ops

## Slide 19: Arc tracks on CS shoulder and divertor tiles
Consistent arcs usually observed during disruptions on fast cameras

## Slide 20: Drips evident on Bay J midplane
Before:
After:
Source ? Leak sealant ?
Remedy ?

## Slide 21: Flaky coating evident on several structures at miplane
Flaky, greasy like surface found on vessel entry
Related to use of Aerodag?
Bay L
Recommend:
Trials of Aerodag to see if it matches
Restrictions and review of in-vessel surfaces after Aerodag use
Note Bay B QMB developed ground fault and needed to be disconnected during plasma ops
Bay B QMB shutter

## Slide 22: Flaky, ‘greasy’ coating evident on several structures at miplane
ME-SXR shutter
No aerodag used

## Slide 23: Flaky, ‘greasy’ coating evident on several structures at miplane
Consider Evans East analysis like it was done for IGI granules?

## Slide 24: NBI armor