| Princeton Plasma Physics Laboratory NSTX Experimental Proposal |  |  |  |
| --- | --- | --- | --- |
| Title: Liquid Lithium Divertor recycling and pumping studies |  |  |  |
| OP-XP-1001 | Revision: | Effective Date: (Approval date unless otherwise stipulated) Expiration Date: (2 yrs. unless otherwise stipulated) |  |
| PROPOSAL APPROVALS |  |  |  |
| Responsible Author: V. A. Soukhanovskii |  |  | Date |
| ATI – ET Group Leader: C. H. Skinner |  |  | Date |
| RLM - Run Coordinator: |  |  | Date |
| Responsible Division: Experimental Research Operations |  |  |  |
| RESTRICTIONS or MINOR MODIFICATIONS (Approved by Experimental Research Operations) |  |  |  |

NSTX EXPERIMENTAL PROPOSAL

| TITLE: LLD recycling and pumping studies | No. OP-XP-1001 |
| --- | --- |
| AUTHORS: V. A. Soukhanovskii, M. Jaworski, J. Kallman, H. W. Kugel, R. Maingi, R. Raman, and NSTX Team | DATE: |

# 1.	Overview of planned experiment

This XP is a part of a series of experiments that aim at characterizing the liquid lithium divertor (LLD) performance. In this experiment, pumping and recycling characteristics of the LLD and the surrounding lower divertor surfaces will be studied as functions of the steady-state core ion density, divertor density, and LLD temperature regime. Additionally, particle containment times (tp*) characterizing pump-out of the edge and SOL density will be measured or inferred using measurements-based particle balance models.

# 2.	Theoretical/ empirical justification

Laboratory measurements (e.g., R. Doerner et al., Nucl. Fusion 42, 1318 (2002)) showed that liquid lithium retention of incident ions is a function of both liquid lithium temperature and ion fluence. This experiment aims at measuring the LLD pumping (i.e. dynamic retention) and recycling processes under a variety of temperature and incident ion flux conditions. A prerequisite to this experiment is XP 1000 by H. W. Kugel et al. The latter XP is expected to address the following points:

- Demonstration of reduced ion density / inventory with “warm” LLD (T=215-240 C) (i.e., pumping vs distance to strike point)

- Operational scenario for proper LLD thermal regime (i.e., temperature vs distance to strike point, NBI power)

- Impurity influx and core content with cold and warm LLD

- LITER evaporation requirements such as evaporation rate and evaporation frequency

# 3.	Experimental run plan

- Steady-state ion density scan and Density pump-out (tp*) measurements

  - Establish a long-pulse H-mode discharge with SGI fueling and “cold” LLD (2-3 shots)

- Use SGI scenarios from shots 134134, 134136, 134991 as guidance. If shots do not go through, use 200-400 Torr in high field side injector. SGI regime: R=158 cm, 5000 Torr, 10 ms pulses.

- Use highest PNBI possible while avoiding b-limiting instabilities (from XP 1000, e.g., 3 MW or 5 MW)

- Use shaping similar to the best discharges with LLD pumping from XP  1000, e.g. high-triangularity with ROSP=0.45 m, or medium triangularity with ROSP=0.63 m. Use isoflux control for GAPOUT=10 cm

- Use best LITER scenario established in XP 1000

  - Obtain several reference discharges with cold LLD and several core ion density (ion inventory) values by adding or removing SGI pulses in the fueling scenario (up to 10 shots)

  - Expected range of steady-state ion densities 1-6 x 1019 m-3

  - Obtain core, edge, SOL, and divertor ion and electron densities from multiple diagnostics for particle balance analysis

  - Add 1-3 SGI pulses after 0.4-0.5 s for “pump-out” characterization

  - Repeat best discharges from 1.2 with “warm” LLD to document density behavior (up to 10-15 shots)

    - Use LDGIS gas injection in flat-top phase in 1-3 shots to document divertor density pump-out. LDGIS setup: plenum pressure 200-400 Torr.

- (Optional, time permitting) LLD pumping as function of LLD temperature (up to 15 shots). If technically possible and administratively allowed, characterize pumping and recycling with LLD at higher temperature.

    - Desirable range of LLD temperatures 200-320 C

    - Repeat best discharges from 1.2 and 1.3 with LLD at higher temperature

    - If LLD higher temperature is obtained as a result of plasma heating during a discharge, assure that best SGI pulse scenarios were used for pump-out characterization (parts

    - Optional, time-permitting – repeat 1.3.1 for divertor pump-out characterization

  - (Optional, time-permitting) Density pumping and pump-out (tp*) measurements with warm LLD without fresh LITER coatings.

    - Establish “no-LITER” conditions by running up to 4 discharges without depositing fresh lithium coatings from LITERs. Note divertor recycling and lithium emission changes. Keep the LLD at room temperature for in discharges.

    - Repeat best discharges from 1.2 and 1.3 with “warm” LLD (220-250 C).

# 4.	Required machine, NBI, RF, CHI and diagnostic capabilities

Prerequisite: XP 1000 as described in Section 2.

# 5.	Planned analysis

EFIT, TRANSP, particle balance equations, UEDGE, SOLPS, DEGAS 2

# 6.	Planned publication of results

Results will be presented in upcoming fusion meetings and major refereed publications.

PHYSICS OPERATIONS REQUEST

| TITLE: LLD recycling and pumping studies | No. OP-XP-1001 |
| --- | --- |
| AUTHORS: V. A. Soukhanovskii et al. | DATE: |

Brief description of the most important operational plasma conditions required: Section 1.1

Previous shot(s) which can be repeated: Previous shot(s) which can be modified: 134134, 134136, 134991 and shots from XP 1000

Machine conditions (specify ranges as appropriate, strike out inapplicable cases) ITF (kA): Flattop start/stop (s): IP (MA): Flattop start/stop (s): Configuration: Limiter / DN / LSN / USN Equilibrium Control: Outer gap / Isoflux (rtEFIT) / Strike-point control (rtEFIT) Outer gap (m): Inner gap (m): Z position (m): Elongation: Triangularity (U/L): OSP radius (m): Gas Species: Injector(s): NBI Species: D Voltage (kV) A: B: C: Duration (s): ICRF Power (MW): Phase between straps (°): Duration (s): CHI: Off / On Bank capacitance (mF): LITERs: Off / On Total deposition rate (mg/min): LLD: Temperature (°C): EFC coils: Off/On Configuration: Odd / Even / Other

DIAGNOSTIC CHECKLIST

| TITLE: LLD recycling and pumping studies | No. OP-XP-1001 |
| --- | --- |
| AUTHORS: V. A. Soukhanovskii et al. | DATE: |

Note special diagnostic requirements in Sec. 4

| Diagnostic | Need | Want |
| --- | --- | --- |
| Beam Emission Spectroscopy |  |  |
| Bolometer – divertor |  | √ |
| Bolometer – midplane array |  | √ |
| CHERS – poloidal |  | √ |
| CHERS – toroidal | √ |  |
| Dust detector |  |  |
| Edge deposition monitors |  |  |
| Edge neutral density diag. |  | √ |
| Edge pressure gauges | √ |  |
| Edge rotation diagnostic |  | √ |
| Fast cameras – divertor/LLD | √ |  |
| Fast ion D_alpha - FIDA |  |  |
| Fast lost ion probes - IFLIP |  |  |
| Fast lost ion probes - SFLIP |  |  |
| Filterscopes | √ |  |
| FIReTIP |  | √ |
| Gas puff imaging – divertor |  |  |
| Gas puff imaging – midplane |  |  |
| H camera - 1D | √ |  |
| High-k scattering |  |  |
| Infrared cameras | √ |  |
| Interferometer - 1 mm |  |  |
| Langmuir probes – divertor | √ |  |
| Langmuir probes – LLD | √ |  |
| Langmuir probes – bias tile |  | √ |
| Langmuir probes – RF ant. |  | √ |
| Magnetics – B coils | √ |  |
| Magnetics – Diamagnetism |  |  |
| Magnetics – Flux loops | √ |  |
| Magnetics – Locked modes |  |  |
| Magnetics – Rogowski coils | √ |  |
| Magnetics – Halo currents |  |  |
| Magnetics – RWM sensors |  |  |
| Mirnov coils – high f. |  |  |
| Mirnov coils – poloidal array |  |  |
| Mirnov coils – toroidal array |  |  |
| Mirnov coils – 3-axis proto. |  |  |

Note special diagnostic requirements in Sec. 4

| Diagnostic | Need | Want |
| --- | --- | --- |
| MSE |  |  |
| NPA – E¦¦B scanning |  |  |
| NPA – solid state |  |  |
| Neutron detectors |  |  |
| Plasma TV | √ |  |
| Reflectometer – 65GHz |  |  |
| Reflectometer – correlation |  |  |
| Reflectometer – FM/CW |  |  |
| Reflectometer – fixed f |  |  |
| Reflectometer – SOL |  | √ |
| RF edge probes |  |  |
| Spectrometer – divertor |  | √ |
| Spectrometer – SPRED |  | √ |
| Spectrometer – VIPS |  | √ |
| Spectrometer – LOWEUS |  | √ |
| Spectrometer – XEUS |  | √ |
| SWIFT – 2D flow |  |  |
| Thomson scattering | √ |  |
| Ultrasoft X-ray – pol. arrays |  |  |
| Ultrasoft X-rays – bicolor |  |  |
| Ultrasoft X-rays – TG spectr. |  | √ |
| Visible bremsstrahlung det. |  | √ |
| X-ray crystal spectrom. - H |  |  |
| X-ray crystal spectrom. - V |  |  |
| X-ray tang. pinhole camera |  |  |