| Princeton Plasma Physics Laboratory NSTX Experimental Proposal |  |  |  |
| --- | --- | --- | --- |
| Li pumping and retention on NSTX |  |  |  |
| OP-XP-824 | Revision: | Effective Date: (Approval date unless otherwise stipulated) Expiration Date: (2 yrs. unless otherwise stipulated) |  |
| PROPOSAL APPROVALS |  |  |  |
| Responsible Author: Charles Skinner |  |  | Date: 7 April 2008 |
| ATI – ET Group Leader: Vlad Soukhanovskii |  |  | Date |
| RLM - Run Coordinator: Michael Bell |  |  | Date |
| Responsible Division: Experimental Research Operations |  |  |  |
| Chit Review Board (designated by Run Coordinator) |  |  |  |
| MINOR MODIFICATIONS (Approved by Experimental Research Operations) |  |  |  |

NSTX EXPERIMENTAL PROPOSAL

| TITLE: Li pumping and retention on NSTX – part 1 | No. OP-XP-824 |
| --- | --- |
| AUTHORS: C. H. Skinner, R. Maingi, V. Soukhanovski, W. Blanchard | DATE: 4/9/08 |

# 1.	Overview of planned experiment

Briefly describe the scientific goals of the experiment.

- To measure the fraction of the injected deuterium that is retained in the NSTX vessel both with and without PFCs coated with fresh (active) lithium.

- The measurement will compare the static pressure rise in the vessel after ohmic and RF discharges with the pressure rise in the vessel in a gas-only shot, all with the valves closed.

- This XP focusses on measuring retention before LiTER operations. Retention will be dominated by D implantation followed by outgassing. QMB measurements have shown that codeposition is small in the short term. A subsequent XP will address retetion during LiTER operations.

# 2.	Theoretical/ empirical justification

Brief justification of activity, including supporting calculations as appropriate. Describe briefly any previous or related experiments.

This is important information for the NSTX lithium program which aims at density control via a reduction in the recycling of hydrogenic species using lithium pellet injection and lithium evaporation. It is also needed for the Joint US tokamak FY 2009 milestone on pumping and retention. 
This aims to “Conduct experiments on major fusion facilities to develop understanding of particle control and  hydrogenic fuel retention in tokamaks. In FY09, FES will identify the fundamental processes  governing particle balance by systematically investigating a combination of divertor geometries,  particle exhaust capabilities, and wall materials.  Alcator C-mod operates with high-Z metal walls,  NSTX is pursuing the use of lithium surfaces in the divertor, and DIII-D continues operating with all  graphite walls.  Edge diagnostics measuring the heat and particle flux to walls and divertor  surfaces, coupled with plasma profile data and material surface analysis, will provide input for  validating simulation codes.  The results achieved will be used to improve extrapolations to  planned ITER operation.

(* text updated, shown as accepted by DoE)

# 3.	Experimental run plan

Describe experiment in detail, including decision points and processes.

- Assume previous XP ends with standard He-GDC

- 2-3  Gas only shots 2 puff (128266) and 4 puff (128268) to establish baseline ‘retention’ < 1%. 
If > 1% repeat one gas-only shot then continue.

- 3-5 shots discharge development:

  - Use RF conditioning shot #128133 as starting point to develop and reproduce non-disruptive ohmic discharges (0.5-0.6 MA) with 100-200 ms flattop, and controlled rampdown.

  - Drop Bt to 0.45 T. Ramp down current before OH runs out e.g. at 0.5 s to make sure it is smooth. Replace HFS gas puff with more gas from injector #2.

  - NB valve is always closed. TMP valves closed 30 s before shot (RGA valve stays open).

  - Leave valves closed for 5 mins after each discharge.

  - Follow with He-GDC. Establish minimum He-GDC needed for reproducible discharges.

- 1-shot repeat of optimal ohmic discharge.

- 1 shot repeat of gas-only shot at closest IG_110 pressure. 7-10 shots so far.

- 3 shots RF discharge 0.65 mA, 1.5 MW RF power (enough for H-mode ?). Use ohmic discharges as baseline, with steady RF power added during flattop and maybe part of ramp up.

- 1 shot repeat of gas-only discharge.

- 1-shot repeat of optimal RF discharge. Last shot of the day - keep TMP (and NB) TVIs closed for 24+ hrs to monitor long term outgassing.

- Total 12-15 shots. If there is no time for RF part still keep TMP closed after final ohmic shot.

- Repeat above during LiTER operation to measure retention fraction with fresh lithium coating and 10, 20, 30 minutes after LiTER shutter closed.

# 4.	Required machine, NBI, RF, CHI and diagnostic capabilities

Describe any prerequisite conditions, development, XPs or XMPs needed.
Attach completed Physics Operations Request and Diagnostic Checklist.

Prior to running this XP, the feasibility of separating the He and D contributions to the total pressure should be demonstrated using variable mixtures of He and D puffed from the NSTX fueling system.

- Ion Gauges.

- Sensotec for Inj. #2.

- Trend RGA trend and shot RGA.

- Penning gauge.

- Infrared camera

- Bolometers

- 1D H camera

- Quartz Microbalances.

Needed for simulations:

- TS

- CHERS

- Langmuir probe – BeaP

- Edge neutral density diagnostic

- GPI for Te fluctuations.

Pending:

- Penning gauge piggy back data (Vlad / Mark Cropper).

- Penning gauge data from He & D gas-only shots.

- IG and IG_110 trending data from Paul Sichta.

- RGA data transfer to MDS tree. Data is on PC - transfer can be done later (Dana).

- Piggy back data on RGA impurity fraction with higher power NBI if available (Blanchard).

# 5.	Planned analysis

What analysis of the data will be required: EFIT, TRANSP, etc.?

DEGAS, UEDGE….

# 6.	Planned publication of results

What will be the final disposition of the results; where will results be published and when?

Presentations at DPP APS & ITPA Div/Sol Group. Joint publication with other tokamaks.

PHYSICS OPERATIONS REQUEST

| TITLE: Li pumping and retention on NSTX | No. OP-XP-824 |
| --- | --- |
| AUTHORS: C. H. Skinner, R. Maingi, V. Soukhanovski, W. Blanchard | DATE: 4/8/08 |

Machine conditions (specify ranges as appropriate)

ITF (kA): ?	Flattop start/stop (s):  ?

IP (MA): 500 - 600	Flattop start/stop (s): 100 ms – 300 ms

Configuration: Limiter / DN / LSN / USN	LSN

Outer gap (m): 	?	Inner gap (m): 	?

Elongation :	?	Upper/lower triangularity :	?

Z position (m):	?

Gas Species: 	Deuterium	Injector(s):  #2

NBI Species: D	Sources: 	 none	Voltage (kV): 		Duration (s):

ICRF Power (MW):	 1.5 MW	Phasing: 	?	Duration (s): ?

CHI:	On / Off	OFF Bank capacitance (mF):

LITER:  On / Off   OFF

Either:	List previous shot numbers for setup:	128133

Or:	Sketch the desired time profiles, including inner and outer gaps, , , heating, fuelling, etc. as appropriate. Accurately label the sketch with times and values.

DIAGNOSTIC CHECKLIST

| TITLE: Li pumping and retention on NSTX | No. OP-XP-824 |
| --- | --- |
| AUTHORS: C. H. Skinner, R. Maingi, V. Soukhanovski, W. Blanchard | DATE: 4/7/08 |

Note special diagnostic requirements in Sec. 4

| Diagnostic | Need | Want |
| --- | --- | --- |
| Bolometer – tangential array |  | √ |
| Bolometer – divertor |  | √ |
| CHERS – toroidal | √ |  |
| CHERS – poloidal |  | √ |
| Divertor fast camera |  | √ |
| Dust detector |  | √ |
| EBW radiometers |  |  |
| Edge deposition monitors | √ |  |
| Edge neutral density diag. | √ |  |
| Edge pressure gauges | √ |  |
| Edge rotation diagnostic |  | √ |
| Fast ion D_alpha - FIDA |  |  |
| Fast lost ion probes - IFLIP |  |  |
| Fast lost ion probes - SFLIP |  |  |
| Filterscopes | √ |  |
| FIReTIP |  |  |
| Gas puff imaging | √ |  |
| H camera - 1D | √ |  |
| High-k scattering |  |  |
| Infrared cameras | √ |  |
| Interferometer - 1 mm |  |  |
| Langmuir probes – divertor | √ |  |
| Langmuir probes – BEaP | √ |  |
| Langmuir probes – RF ant. | √ |  |
| Magnetics – Diamagnetism |  |  |
| Magnetics – Flux loops | √ |  |
| Magnetics – Locked modes |  |  |
| Magnetics – Pickup coils | √ |  |
| Magnetics – Rogowski coils | √ |  |
| Magnetics – Halo currents |  |  |
| Magnetics – RWM sensors |  |  |
| Mirnov coils – high f. |  |  |
| Mirnov coils – poloidal array |  |  |
| Mirnov coils – toroidal array |  |  |
| Mirnov coils – 3-axis proto. |  |  |

Note special diagnostic requirements in Sec. 4

| Diagnostic | Need | Want |
| --- | --- | --- |
| MSE |  |  |
| NPA – ExB scanning |  |  |
| NPA – solid state |  |  |
| Neutron measurements |  |  |
| Plasma TV |  | √ |
| Reciprocating probe | √ |  |
| Reflectometer – 65GHz |  |  |
| Reflectometer – correlation |  |  |
| Reflectometer – FM/CW |  |  |
| Reflectometer – fixed f |  |  |
| Reflectometer – SOL |  |  |
| RF edge probes |  |  |
| Spectrometer – SPRED |  | √ |
| Spectrometer – VIPS |  | √ |
| SWIFT – 2D flow |  |  |
| Thomson scattering | √ |  |
| Ultrasoft X-ray arrays |  |  |
| Ultrasoft X-rays – bicolor |  |  |
| Ultrasoft X-rays – TG spectr. |  |  |
| Visible bremsstrahlung det. |  | √ |
| X-ray crystal spectrom. - H |  |  |
| X-ray crystal spectrom. - V |  |  |
| X-ray fast pinhole camera |  |  |
| X-ray spectrometer - XEUS |  | √ |
| Ionization gauges | √ |  |
| Penning gauge | √ |  |
| RGA | √ |  |
| shotRGA | √ |  |